6 Etosha 18 Ssub 2-5 cm S1 550C

Graphics

Graphics

Graphics

Quantitative Results

Phase Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide

Weight fraction/ %	29.0

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	30.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	29.0

Phase Sodium Magnesium Silicon Oxide Hydrate

Weight fraction/ %	12.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | Sodium Aluminum Silicate Hydrate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Sodium Magnesium Silicon Oxide Hydrate |
| --- | --- | --- | --- | --- |
| 6 Etosha18 Ssub 2-5cm S1 550C | 29.0 | 30.0 | 29.0 | 12.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 7057.0000 | 7046.4802 | 7057.0000 |
| 2.0164 | 7024.6480 | 7011.1908 | 7011.1908 |
| 2.0274 | 6915.5329 | 6965.3816 | 6965.3816 |
| 2.0384 | 6892.5015 | 6919.5724 | 6919.5724 |
| 2.0494 | 6779.0806 | 6873.7632 | 6873.7632 |
| 2.0604 | 6853.5752 | 6827.9540 | 6827.9540 |
| 2.0714 | 6780.2478 | 6782.1448 | 6782.1448 |
| 2.0824 | 6697.1593 | 6736.3356 | 6736.3356 |
| 2.0934 | 6577.9685 | 6690.5264 | 6690.5264 |
| 2.1044 | 6545.5354 | 6644.7172 | 6644.7172 |
| 2.1154 | 6583.1062 | 6598.9080 | 6598.9080 |
| 2.1264 | 6593.1632 | 6553.0988 | 6553.0988 |
| 2.1374 | 6561.1298 | 6507.2896 | 6507.2896 |
| 2.1484 | 6299.1957 | 6461.4804 | 6461.4804 |
| 2.1594 | 6326.6686 | 6415.6712 | 6415.6712 |
| 2.1704 | 6364.9100 | 6369.8620 | 6369.8620 |
| 2.1814 | 6319.7827 | 6324.0528 | 6324.0528 |
| 2.1924 | 6338.5683 | 6280.8947 | 6278.2436 |
| 2.2034 | 6194.7434 | 6243.9785 | 6243.9785 |
| 2.2144 | 6129.5629 | 6209.7134 | 6209.7134 |
| 2.2254 | 6120.6539 | 6175.4482 | 6175.4482 |
| 2.2364 | 6149.6150 | 6141.1831 | 6141.1831 |
| 2.2474 | 6131.6234 | 6106.9180 | 6106.9180 |
| 2.2584 | 5992.1519 | 6072.6528 | 6072.6528 |
| 2.2694 | 5993.5398 | 6038.3877 | 6038.3877 |
| 2.2804 | 5993.3963 | 6004.1225 | 6004.1225 |
| 2.2914 | 5999.2458 | 5969.8574 | 5969.8574 |
| 2.3024 | 6010.5221 | 5935.5923 | 5935.5923 |
| 2.3134 | 5907.7925 | 5901.3271 | 5901.3271 |
| 2.3244 | 5875.7129 | 5867.0620 | 5867.0620 |
| 2.3354 | 5851.5575 | 5832.7968 | 5832.7968 |
| 2.3464 | 5787.4248 | 5798.5317 | 5798.5317 |
| 2.3574 | 5715.0619 | 5764.2666 | 5764.2666 |
| 2.3684 | 5716.2463 | 5730.0014 | 5730.0014 |
| 2.3794 | 5740.8082 | 5696.5336 | 5695.7363 |
| 2.3904 | 5653.8717 | 5664.9432 | 5664.9432 |
| 2.4014 | 5625.3717 | 5634.1500 | 5634.1500 |
| 2.4124 | 5612.1052 | 5603.3569 | 5603.3569 |
| 2.4234 | 5625.5152 | 5572.5637 | 5572.5637 |
| 2.4344 | 5543.4779 | 5541.7706 | 5541.7706 |
| 2.4454 | 5409.7119 | 5510.9774 | 5510.9774 |
| 2.4564 | 5400.5035 | 5480.1843 | 5480.1843 |
| 2.4674 | 5453.1593 | 5449.3912 | 5449.3912 |
| 2.4784 | 5420.8024 | 5418.5980 | 5418.5980 |
| 2.4894 | 5331.7768 | 5387.8049 | 5387.8049 |
| 2.5004 | 5334.9469 | 5357.0117 | 5357.0117 |
| 2.5114 | 5353.3382 | 5326.2186 | 5326.2186 |
| 2.5224 | 5296.0723 | 5295.4255 | 5295.4255 |
| 2.5334 | 5263.1504 | 5264.6323 | 5264.6323 |
| 2.5444 | 5253.9887 | 5233.8392 | 5233.8392 |
| 2.5554 | 5256.9164 | 5203.0460 | 5203.0460 |
| 2.5664 | 5199.8230 | 5172.2529 | 5172.2529 |
| 2.5774 | 5110.9518 | 5141.4597 | 5141.4597 |
| 2.5884 | 5183.9253 | 5110.6666 | 5110.6666 |
| 2.5994 | 5118.8672 | 5079.8735 | 5079.8735 |
| 2.6104 | 4987.0192 | 5049.0803 | 5049.0803 |
| 2.6214 | 4930.9744 | 5018.2872 | 5018.2872 |
| 2.6324 | 4869.8569 | 4987.4940 | 4987.4940 |
| 2.6434 | 4890.7729 | 4956.7009 | 4956.7009 |
| 2.6544 | 4889.1455 | 4925.9077 | 4925.9077 |
| 2.6654 | 4854.7139 | 4895.1146 | 4895.1146 |
| 2.6764 | 4746.0324 | 4864.3215 | 4864.3215 |
| 2.6874 | 4724.4307 | 4833.5283 | 4833.5283 |
| 2.6984 | 4787.6239 | 4802.7352 | 4802.7352 |
| 2.7094 | 4917.4877 | 4771.9420 | 4771.9420 |
| 2.7204 | 4733.0909 | 4741.1489 | 4741.1489 |
| 2.7314 | 4730.1062 | 4710.3558 | 4710.3558 |
| 2.7424 | 4703.2955 | 4679.5626 | 4679.5626 |
| 2.7534 | 4621.4503 | 4648.8419 | 4648.7695 |
| 2.7644 | 4643.4676 | 4618.2916 | 4618.2916 |
| 2.7754 | 4557.9400 | 4587.8137 | 4587.8137 |
| 2.7864 | 4594.4872 | 4557.3358 | 4557.3358 |
| 2.7974 | 4467.4867 | 4526.8580 | 4526.8580 |
| 2.8084 | 4613.2989 | 4496.3801 | 4496.3801 |
| 2.8194 | 4495.5693 | 4465.9022 | 4465.9022 |
| 2.8304 | 4480.1563 | 4435.4243 | 4435.4243 |
| 2.8414 | 4385.6539 | 4404.9464 | 4404.9464 |
| 2.8524 | 4281.5197 | 4374.4686 | 4374.4686 |
| 2.8634 | 4171.5015 | 4343.9907 | 4343.9907 |
| 2.8744 | 4323.3299 | 4313.5128 | 4313.5128 |
| 2.8854 | 4334.8830 | 4283.0349 | 4283.0349 |
| 2.8964 | 4233.4513 | 4252.5570 | 4252.5570 |
| 2.9074 | 4229.5909 | 4222.0792 | 4222.0792 |
| 2.9184 | 4175.4803 | 4191.6013 | 4191.6013 |
| 2.9294 | 4053.6165 | 4161.1234 | 4161.1234 |
| 2.9404 | 4075.5344 | 4131.5742 | 4130.6455 |
| 2.9514 | 4161.3225 | 4104.2116 | 4104.2116 |
| 2.9624 | 4312.9365 | 4077.7777 | 4077.7777 |
| 2.9734 | 4047.0432 | 4051.3439 | 4051.3439 |
| 2.9844 | 3947.9587 | 4024.9100 | 4024.9100 |
| 2.9954 | 4059.3009 | 3998.4761 | 3998.4761 |
| 3.0064 | 3937.1278 | 3972.0422 | 3972.0422 |
| 3.0174 | 3876.1917 | 3945.6083 | 3945.6083 |
| 3.0284 | 3829.7419 | 3919.1745 | 3919.1745 |
| 3.0394 | 3938.5821 | 3892.7406 | 3892.7406 |
| 3.0504 | 3911.9528 | 3866.3067 | 3866.3067 |
| 3.0614 | 3875.4189 | 3839.8728 | 3839.8728 |
| 3.0724 | 3877.1593 | 3813.4389 | 3813.4389 |
| 3.0834 | 3799.3658 | 3787.0050 | 3787.0050 |
| 3.0944 | 3719.0973 | 3760.5712 | 3760.5712 |
| 3.1054 | 3703.6254 | 3734.1373 | 3734.1373 |
| 3.1164 | 3710.8284 | 3707.7034 | 3707.7034 |
| 3.1274 | 3717.5575 | 3683.6674 | 3681.2695 |
| 3.1384 | 3638.3732 | 3665.2774 | 3665.2774 |
| 3.1494 | 3626.3726 | 3649.2853 | 3649.2853 |
| 3.1604 | 3561.6785 | 3633.2932 | 3633.2932 |
| 3.1714 | 3617.0865 | 3617.3010 | 3617.3010 |
| 3.1824 | 3515.6849 | 3601.3089 | 3601.3089 |
| 3.1934 | 3551.3452 | 3585.3168 | 3585.3168 |
| 3.2044 | 3611.7316 | 3569.3247 | 3569.3247 |
| 3.2154 | 3556.5428 | 3553.3326 | 3553.3326 |
| 3.2264 | 3502.7212 | 3537.3404 | 3537.3404 |
| 3.2374 | 3477.0403 | 3521.3483 | 3521.3483 |
| 3.2484 | 3394.6111 | 3505.3562 | 3505.3562 |
| 3.2594 | 3373.1652 | 3489.3641 | 3489.3641 |
| 3.2704 | 3487.5969 | 3473.3720 | 3473.3720 |
| 3.2814 | 3510.5634 | 3457.3799 | 3457.3799 |
| 3.2924 | 3458.9071 | 3441.3877 | 3441.3877 |
| 3.3034 | 3432.0531 | 3425.3956 | 3425.3956 |
| 3.3144 | 3445.7901 | 3409.4035 | 3409.4035 |
| 3.3254 | 3411.8318 | 3393.4114 | 3393.4114 |
| 3.3364 | 3326.9459 | 3377.4193 | 3377.4193 |
| 3.3474 | 3330.9587 | 3361.4272 | 3361.4272 |
| 3.3584 | 3276.7817 | 3345.4350 | 3345.4350 |
| 3.3694 | 3244.2222 | 3329.4429 | 3329.4429 |
| 3.3804 | 3292.6362 | 3313.4508 | 3313.4508 |
| 3.3914 | 3259.4690 | 3297.4587 | 3297.4587 |
| 3.4024 | 3219.7320 | 3281.4666 | 3281.4666 |
| 3.4134 | 3251.1406 | 3265.4744 | 3265.4744 |
| 3.4244 | 3281.0723 | 3249.4823 | 3249.4823 |
| 3.4354 | 3225.1947 | 3233.4902 | 3233.4902 |
| 3.4464 | 3178.0177 | 3217.4981 | 3217.4981 |
| 3.4574 | 3182.8260 | 3201.5060 | 3201.5060 |
| 3.4684 | 3148.7438 | 3185.5139 | 3185.5139 |
| 3.4794 | 3138.5870 | 3169.5217 | 3169.5217 |
| 3.4904 | 3143.3628 | 3153.5296 | 3153.5296 |
| 3.5014 | 3121.8525 | 3138.0425 | 3137.5375 |
| 3.5124 | 3178.3358 | 3123.7444 | 3123.7444 |
| 3.5234 | 3082.2979 | 3109.9512 | 3109.9512 |
| 3.5344 | 3112.0148 | 3096.1581 | 3096.1581 |
| 3.5454 | 3089.3402 | 3082.3677 | 3082.3650 |
| 3.5564 | 3082.3938 | 3068.6919 | 3068.5719 |
| 3.5674 | 3079.0560 | 3054.9016 | 3054.7787 |
| 3.5784 | 3053.2714 | 3041.1693 | 3040.9856 |
| 3.5894 | 3013.6637 | 3027.3786 | 3027.1925 |
| 3.6004 | 3007.9110 | 3013.5879 | 3013.3993 |
| 3.6114 | 2992.3156 | 2999.7972 | 2999.6062 |
| 3.6224 | 2912.1622 | 2986.0066 | 2985.8131 |
| 3.6334 | 2866.1514 | 2972.2160 | 2972.0200 |
| 3.6444 | 2909.8820 | 2958.4255 | 2958.2268 |
| 3.6554 | 2893.0029 | 2944.6351 | 2944.4337 |
| 3.6664 | 2864.0334 | 2930.8447 | 2930.6406 |
| 3.6774 | 2914.6991 | 2917.0543 | 2916.8474 |
| 3.6884 | 2911.5531 | 2903.9885 | 2903.0543 |
| 3.6994 | 2910.0000 | 2892.6287 | 2892.4161 |
| 3.7104 | 2878.3210 | 2881.9934 | 2881.7779 |
| 3.7214 | 2889.6785 | 2871.3582 | 2871.1396 |
| 3.7324 | 2950.5005 | 2860.7231 | 2860.5014 |
| 3.7434 | 2817.4700 | 2850.0880 | 2849.8632 |
| 3.7544 | 2824.2684 | 2839.4530 | 2839.2250 |
| 3.7654 | 2797.9361 | 2828.8181 | 2828.5868 |
| 3.7764 | 2758.8245 | 2818.1832 | 2817.9485 |
| 3.7874 | 2815.4867 | 2807.5484 | 2807.3103 |
| 3.7984 | 2743.0447 | 2796.9137 | 2796.6721 |
| 3.8094 | 2756.0787 | 2786.2791 | 2786.0339 |
| 3.8204 | 2761.3643 | 2775.6445 | 2775.3956 |
| 3.8314 | 2772.1858 | 2765.0101 | 2764.7574 |
| 3.8424 | 2731.0516 | 2754.3757 | 2754.1192 |
| 3.8534 | 2771.7640 | 2743.7414 | 2743.4810 |
| 3.8644 | 2811.6430 | 2733.1072 | 2732.8428 |
| 3.8754 | 2645.7267 | 2722.4731 | 2722.2045 |
| 3.8864 | 2710.7168 | 2711.8390 | 2711.5663 |
| 3.8974 | 2759.8485 | 2701.2051 | 2700.9281 |
| 3.9084 | 2682.5162 | 2690.5713 | 2690.2899 |
| 3.9194 | 2700.2095 | 2679.9376 | 2679.6516 |
| 3.9304 | 2721.4542 | 2669.3040 | 2669.0134 |
| 3.9414 | 2588.6735 | 2658.6705 | 2658.3752 |
| 3.9524 | 2588.2286 | 2648.0371 | 2647.7370 |
| 3.9634 | 2600.1977 | 2637.4039 | 2637.0988 |
| 3.9744 | 2622.5978 | 2626.7708 | 2626.4605 |
| 3.9854 | 2617.3186 | 2616.1378 | 2615.8223 |
| 3.9964 | 2645.4749 | 2605.5049 | 2605.1841 |
| 4.0074 | 2589.2655 | 2594.8722 | 2594.5459 |
| 4.0184 | 2575.5811 | 2584.2396 | 2583.9076 |
| 4.0294 | 2503.4622 | 2573.6071 | 2573.2694 |
| 4.0404 | 2517.9385 | 2562.9749 | 2562.6312 |
| 4.0514 | 2520.9204 | 2552.3427 | 2551.9930 |
| 4.0624 | 2603.2306 | 2542.0894 | 2541.3548 |
| 4.0734 | 2522.6283 | 2532.2331 | 2531.8707 |
| 4.0844 | 2498.8407 | 2522.7556 | 2522.3866 |
| 4.0954 | 2522.4877 | 2513.2783 | 2512.9025 |
| 4.1064 | 2478.6844 | 2503.8012 | 2503.4185 |
| 4.1174 | 2494.8849 | 2494.3243 | 2493.9344 |
| 4.1284 | 2471.3496 | 2484.8476 | 2484.4503 |
| 4.1394 | 2477.3845 | 2475.3711 | 2474.9663 |
| 4.1504 | 2459.3525 | 2465.8949 | 2465.4822 |
| 4.1614 | 2416.6834 | 2456.4188 | 2455.9981 |
| 4.1724 | 2380.4105 | 2446.9430 | 2446.5141 |
| 4.1834 | 2392.3894 | 2437.4674 | 2437.0300 |
| 4.1944 | 2419.0551 | 2427.9921 | 2427.5459 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 6 Etosha18 Ssub 2-5cm S1 550C | 2.0054 | 29.9894 | 0.0110 | 12/7/2023 11:57:10 AM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 5.2876 | 127.62 | 0.1732 | 16.69961 | 10.55 |
| 8.7139 | 1209.31 | 0.0649 | 10.13949 | 100.00 |
| 10.5865 | 114.09 | 0.4330 | 8.34984 | 9.43 |
| 16.0386 | 601.19 | 0.2165 | 5.52161 | 49.71 |
| 17.6681 | 73.72 | 0.6927 | 5.01585 | 6.10 |
| 19.6258 | 74.21 | 0.5196 | 4.51970 | 6.14 |
| 20.2282 | 75.10 | 0.2598 | 4.38645 | 6.21 |
| 22.4366 | 42.18 | 0.2598 | 3.95944 | 3.49 |
| 24.6105 | 29.52 | 0.2598 | 3.61439 | 2.44 |
| 26.3135 | 556.76 | 0.1299 | 3.38420 | 46.04 |
| 27.5048 | 177.62 | 0.3464 | 3.24028 | 14.69 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-017-4317 | 56 | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | K Mg0.2 Mn0.1 Fe2.4 Al1.7 Si2.6 O10 ( O H )2 | Biotite-1M | 29 |
| * | 01-076-6569 | 20 | Sodium Aluminum Silicate Hydrate | Na0.9 ( ( Al0.9 Si2 ) O6 ) ( H2 O ) | Analcime | 30 |
| * | 04-025-4215 | 2 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 29 |
| * | 01-082-8023 | 1 | Sodium Magnesium Silicon Oxide Hydrate | Na2 Mg3 ( Si6 O16 ) ( H2 O )7 | Loughlinite | 12 |

Anchor Scan Parameters

Dataset Name	6 Etosha18 Ssub 2-5cm S1 550C

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 6\6 Etosha18 Ssub 2-5cm S1 550C.xrdml

Sample Identification	6 Etosha18 Ssub 2-5cm S1 550C

Measurement Start Date/Time	12/7/2023 11:57:10 AM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes