7 Etosha 22 RIP 0-1 cm S1 550 C

Graphics

Graphics

Graphics

Quantitative Results

Phase Potassium Sodium Magnesium Manganese Aluminum Iron Titanium Fluoride Aluminum Silicate Hydroxide

Weight fraction/ %	35.0

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	32.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	16.0

Phase Magnesium Aluminum Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	17.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Potassium Sodium Magnesium Manganese Aluminum Iron Titanium Fluoride Aluminum Silicate Hydroxide | Sodium Aluminum Silicate Hydrate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate |
| --- | --- | --- | --- | --- |
| 7 Etosha22 RIP 0-1cm S1 heat 550C | 35.0 | 32.0 | 16.0 | 17.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 6996.0000 | 7610.4447 | 6996.0000 |
| 2.0164 | 7057.3933 | 7667.2248 | 6955.2049 |
| 2.0274 | 7086.9351 | 7679.6575 | 6914.4098 |
| 2.0384 | 7005.6637 | 7661.3921 | 6873.6147 |
| 2.0494 | 7017.3953 | 7607.7566 | 6832.8195 |
| 2.0604 | 6906.9105 | 7521.9126 | 6792.0244 |
| 2.0714 | 6872.9351 | 7413.0644 | 6751.2293 |
| 2.0824 | 6842.0098 | 7292.1804 | 6710.4342 |
| 2.0934 | 6787.6234 | 7168.6625 | 6669.6391 |
| 2.1044 | 6771.1283 | 7049.1745 | 6628.8440 |
| 2.1154 | 6720.0885 | 6937.8217 | 6588.0488 |
| 2.1264 | 6586.1121 | 6836.7071 | 6547.2537 |
| 2.1374 | 6628.1180 | 6746.4532 | 6506.4586 |
| 2.1484 | 6574.5152 | 6666.6355 | 6465.6635 |
| 2.1594 | 6556.3481 | 6596.1589 | 6424.8684 |
| 2.1704 | 6397.3304 | 6533.5853 | 6384.0733 |
| 2.1814 | 6468.2970 | 6477.3983 | 6343.2781 |
| 2.1924 | 6405.5088 | 6426.0292 | 6302.4830 |
| 2.2034 | 6303.5664 | 6378.4942 | 6261.4088 |
| 2.2144 | 6420.3240 | 6333.6538 | 6220.3345 |
| 2.2254 | 6285.7109 | 6290.9831 | 6179.2602 |
| 2.2364 | 6318.4720 | 6250.0051 | 6138.1859 |
| 2.2474 | 6174.9125 | 6210.4062 | 6097.1117 |
| 2.2584 | 6292.2404 | 6171.9908 | 6056.0374 |
| 2.2694 | 6244.2979 | 6134.6438 | 6014.9631 |
| 2.2804 | 6083.7198 | 6098.3032 | 5973.8889 |
| 2.2914 | 6053.9784 | 6062.9397 | 5932.8146 |
| 2.3024 | 6071.0752 | 6028.5445 | 5891.7403 |
| 2.3134 | 6061.4346 | 5995.1201 | 5850.6660 |
| 2.3244 | 6077.7026 | 5962.6754 | 5809.5918 |
| 2.3354 | 6006.7758 | 5931.2218 | 5768.5175 |
| 2.3464 | 5934.4203 | 5900.7703 | 5727.4432 |
| 2.3574 | 5874.1927 | 5871.3296 | 5686.3689 |
| 2.3684 | 5834.1873 | 5842.9043 | 5645.2947 |
| 2.3794 | 5864.1750 | 5815.4931 | 5604.2204 |
| 2.3904 | 5910.7099 | 5789.0871 | 5563.1461 |
| 2.4014 | 5842.9558 | 5763.6687 | 5522.0719 |
| 2.4124 | 5815.8431 | 5739.2094 | 5480.9976 |
| 2.4234 | 5699.8378 | 5715.6690 | 5439.9233 |
| 2.4344 | 5769.6947 | 5692.9934 | 5398.8490 |
| 2.4454 | 5696.5880 | 5671.1132 | 5357.7748 |
| 2.4564 | 5591.9371 | 5649.9417 | 5316.7005 |
| 2.4674 | 5576.7729 | 5629.3731 | 5275.6262 |
| 2.4784 | 5601.1824 | 5609.2803 | 5234.5519 |
| 2.4894 | 5591.1436 | 5589.5128 | 5193.4777 |
| 2.5004 | 5536.3230 | 5569.8947 | 5152.4034 |
| 2.5114 | 5420.7532 | 5550.2225 | 5111.3291 |
| 2.5224 | 5462.1136 | 5530.2644 | 5070.2549 |
| 2.5334 | 5427.2360 | 5509.7593 | 5029.1806 |
| 2.5444 | 5339.1819 | 5488.4191 | 4988.1063 |
| 2.5554 | 5340.3019 | 5465.9318 | 4947.0320 |
| 2.5664 | 5293.4793 | 5441.8063 | 4905.9578 |
| 2.5774 | 5278.0610 | 5415.9122 | 4864.6043 |
| 2.5884 | 5257.9887 | 5387.7126 | 4823.2509 |
| 2.5994 | 5197.2035 | 5357.0600 | 4781.8975 |
| 2.6104 | 5182.7881 | 5323.6845 | 4740.5440 |
| 2.6214 | 5123.6765 | 5287.3727 | 4699.1906 |
| 2.6324 | 5086.5929 | 5247.9828 | 4657.8372 |
| 2.6434 | 5015.2763 | 5205.4554 | 4616.4838 |
| 2.6544 | 4958.2679 | 5159.8179 | 4575.1303 |
| 2.6654 | 4886.5280 | 5111.1823 | 4533.7769 |
| 2.6764 | 4942.9744 | 5059.7365 | 4492.4235 |
| 2.6874 | 4872.2202 | 5005.7309 | 4451.0700 |
| 2.6984 | 4800.9602 | 4949.4612 | 4409.7166 |
| 2.7094 | 4740.2291 | 4891.2507 | 4368.3632 |
| 2.7204 | 4650.3038 | 4831.4341 | 4327.0098 |
| 2.7314 | 4552.3127 | 4770.3426 | 4285.6563 |
| 2.7424 | 4519.1770 | 4708.2934 | 4244.3029 |
| 2.7534 | 4384.7807 | 4645.3820 | 4202.9495 |
| 2.7644 | 4297.9380 | 4582.1317 | 4161.2510 |
| 2.7754 | 4388.5241 | 4518.5280 | 4119.5525 |
| 2.7864 | 4249.6657 | 4454.9816 | 4077.8540 |
| 2.7974 | 4232.3097 | 4391.6755 | 4036.1555 |
| 2.8084 | 4137.8918 | 4328.7659 | 3994.4570 |
| 2.8194 | 4190.6677 | 4266.3845 | 3952.7585 |
| 2.8304 | 4151.8304 | 4204.6406 | 3911.0601 |
| 2.8414 | 4171.3530 | 4143.6231 | 3869.3616 |
| 2.8524 | 3915.5762 | 4083.4025 | 3827.6631 |
| 2.8634 | 3899.0826 | 4024.0324 | 3785.9646 |
| 2.8744 | 3850.4503 | 3965.5515 | 3744.2661 |
| 2.8854 | 3823.4346 | 3907.9847 | 3702.5676 |
| 2.8964 | 3696.5619 | 3851.3448 | 3660.8691 |
| 2.9074 | 3657.1268 | 3795.6338 | 3619.1706 |
| 2.9184 | 3548.3707 | 3740.8439 | 3577.4722 |
| 2.9294 | 3609.7758 | 3686.9589 | 3535.7737 |
| 2.9404 | 3454.2684 | 3639.8557 | 3494.0752 |
| 2.9514 | 3456.9774 | 3591.9873 | 3462.5599 |
| 2.9624 | 3405.8909 | 3550.8367 | 3431.0447 |
| 2.9734 | 3393.2035 | 3510.4651 | 3399.5295 |
| 2.9844 | 3400.4400 | 3470.8311 | 3368.0142 |
| 2.9954 | 3243.8496 | 3431.8910 | 3336.4990 |
| 3.0064 | 3335.5305 | 3393.6002 | 3304.9838 |
| 3.0174 | 3221.5005 | 3355.9133 | 3273.4685 |
| 3.0284 | 3253.1062 | 3318.7853 | 3241.9533 |
| 3.0394 | 3117.3609 | 3282.1720 | 3210.4381 |
| 3.0504 | 3202.2385 | 3246.0303 | 3178.9228 |
| 3.0614 | 3246.4454 | 3210.3189 | 3147.4076 |
| 3.0724 | 3149.8545 | 3174.9986 | 3115.8924 |
| 3.0834 | 3081.4523 | 3140.0321 | 3084.3771 |
| 3.0944 | 3130.8628 | 3105.3849 | 3052.8619 |
| 3.1054 | 3013.2940 | 3071.0246 | 3021.3467 |
| 3.1164 | 2969.0334 | 3036.9217 | 2989.8314 |
| 3.1274 | 2932.6549 | 3010.4461 | 2958.3162 |
| 3.1384 | 2964.7979 | 2982.1482 | 2939.5677 |
| 3.1494 | 2944.7384 | 2961.4305 | 2920.8192 |
| 3.1604 | 2901.5280 | 2940.8758 | 2902.0707 |
| 3.1714 | 2911.8633 | 2920.4660 | 2883.3222 |
| 3.1824 | 2858.4120 | 2900.1851 | 2864.5738 |
| 3.1934 | 2855.8849 | 2880.0190 | 2845.8253 |
| 3.2044 | 2802.4631 | 2859.9550 | 2827.0768 |
| 3.2154 | 2752.2802 | 2839.9821 | 2808.3283 |
| 3.2264 | 2753.2566 | 2820.0907 | 2789.5798 |
| 3.2374 | 2731.9744 | 2800.2722 | 2770.8313 |
| 3.2484 | 2723.9444 | 2780.5192 | 2752.0828 |
| 3.2594 | 2719.3776 | 2760.8252 | 2733.3344 |
| 3.2704 | 2729.5005 | 2741.1846 | 2714.5859 |
| 3.2814 | 2731.4739 | 2721.5924 | 2695.8374 |
| 3.2924 | 2677.6681 | 2702.0444 | 2677.0889 |
| 3.3034 | 2662.5034 | 2682.5367 | 2658.3404 |
| 3.3144 | 2644.4056 | 2666.5822 | 2639.5919 |
| 3.3254 | 2610.8260 | 2649.6981 | 2626.9120 |
| 3.3364 | 2597.1790 | 2635.8450 | 2614.2321 |
| 3.3474 | 2603.4867 | 2622.1696 | 2601.5522 |
| 3.3584 | 2581.1740 | 2608.8446 | 2588.8722 |
| 3.3694 | 2549.0964 | 2595.6056 | 2576.1923 |
| 3.3804 | 2569.2370 | 2582.3902 | 2563.5124 |
| 3.3914 | 2582.8053 | 2569.1967 | 2550.8325 |
| 3.4024 | 2509.1966 | 2556.0240 | 2538.1525 |
| 3.4134 | 2519.4976 | 2542.8709 | 2525.4726 |
| 3.4244 | 2530.9395 | 2529.7363 | 2512.7927 |
| 3.4354 | 2463.3471 | 2516.6192 | 2500.1128 |
| 3.4464 | 2456.7444 | 2503.5186 | 2487.4328 |
| 3.4574 | 2543.4455 | 2490.4337 | 2474.7529 |
| 3.4684 | 2489.6199 | 2477.3638 | 2462.0730 |
| 3.4794 | 2455.6450 | 2464.3081 | 2449.3931 |
| 3.4904 | 2412.6194 | 2451.2658 | 2436.7131 |
| 3.5014 | 2414.2213 | 2438.7525 | 2424.0332 |
| 3.5124 | 2423.5290 | 2426.1100 | 2412.2439 |
| 3.5234 | 2451.6313 | 2413.9952 | 2400.4546 |
| 3.5344 | 2425.3264 | 2401.8916 | 2388.6654 |
| 3.5454 | 2450.0826 | 2389.8407 | 2376.8761 |
| 3.5564 | 2398.5604 | 2377.8397 | 2365.0868 |
| 3.5674 | 2268.9085 | 2365.7895 | 2353.2975 |
| 3.5784 | 2292.8520 | 2353.7687 | 2341.5082 |
| 3.5894 | 2282.7434 | 2341.7164 | 2329.7189 |
| 3.6004 | 2264.6136 | 2329.6727 | 2317.9296 |
| 3.6114 | 2294.5742 | 2317.6373 | 2306.1403 |
| 3.6224 | 2245.7183 | 2305.6097 | 2294.3510 |
| 3.6334 | 2265.5821 | 2293.5897 | 2282.5617 |
| 3.6444 | 2274.6627 | 2281.5770 | 2270.7724 |
| 3.6554 | 2275.8437 | 2269.5713 | 2258.9832 |
| 3.6664 | 2204.9562 | 2257.5723 | 2247.1939 |
| 3.6774 | 2254.6451 | 2245.5797 | 2235.4046 |
| 3.6884 | 2209.4071 | 2235.1248 | 2223.6153 |
| 3.6994 | 2260.9263 | 2223.4898 | 2213.7029 |
| 3.7104 | 2148.5250 | 2213.3921 | 2203.7906 |
| 3.7214 | 2157.1003 | 2203.2998 | 2193.8782 |
| 3.7324 | 2184.1018 | 2193.2129 | 2183.9658 |
| 3.7434 | 2204.8397 | 2183.1311 | 2174.0535 |
| 3.7544 | 2207.9086 | 2173.0542 | 2164.1411 |
| 3.7654 | 2148.0727 | 2162.9821 | 2154.2287 |
| 3.7764 | 2173.4081 | 2152.9146 | 2144.3164 |
| 3.7874 | 2114.5310 | 2142.8515 | 2134.4040 |
| 3.7984 | 2031.3786 | 2132.7927 | 2124.4917 |
| 3.8094 | 2141.6450 | 2122.7380 | 2114.5793 |
| 3.8204 | 2180.9631 | 2112.6873 | 2104.6669 |
| 3.8314 | 2143.9115 | 2102.6404 | 2094.7546 |
| 3.8424 | 2112.8972 | 2092.5973 | 2084.8422 |
| 3.8534 | 2028.7228 | 2082.5578 | 2074.9298 |
| 3.8644 | 2129.4252 | 2072.5217 | 2065.0175 |
| 3.8754 | 2005.9528 | 2063.2656 | 2055.1051 |
| 3.8864 | 2041.8009 | 2053.4114 | 2046.1445 |
| 3.8974 | 2093.0000 | 2044.3369 | 2037.1839 |
| 3.9084 | 2082.6391 | 2035.2655 | 2028.2233 |
| 3.9194 | 2015.0207 | 2026.1970 | 2019.2627 |
| 3.9304 | 2045.2827 | 2017.1315 | 2010.3021 |
| 3.9414 | 2063.2478 | 2008.0687 | 2001.3415 |
| 3.9524 | 2004.2286 | 1999.0086 | 1992.3809 |
| 3.9634 | 2008.3097 | 1989.9512 | 1983.4203 |
| 3.9744 | 1981.9906 | 1980.8963 | 1974.4597 |
| 3.9854 | 1931.0620 | 1971.8440 | 1965.4991 |
| 3.9964 | 2013.4400 | 1962.7940 | 1956.5385 |
| 4.0074 | 1960.4120 | 1953.7464 | 1947.5779 |
| 4.0184 | 1931.6770 | 1944.7011 | 1938.6173 |
| 4.0294 | 1985.5988 | 1935.6580 | 1929.6567 |
| 4.0404 | 1920.3323 | 1926.6171 | 1920.6961 |
| 4.0514 | 1926.6107 | 1917.5783 | 1911.7355 |
| 4.0624 | 1949.4296 | 1909.8063 | 1902.7749 |
| 4.0734 | 1837.9892 | 1901.0569 | 1895.3642 |
| 4.0844 | 1853.8540 | 1893.5740 | 1887.9535 |
| 4.0954 | 1913.2409 | 1886.0932 | 1880.5428 |
| 4.1064 | 1898.6844 | 1878.6142 | 1873.1322 |
| 4.1174 | 1902.6489 | 1871.1370 | 1865.7215 |
| 4.1284 | 1851.7670 | 1863.6617 | 1858.3108 |
| 4.1394 | 1862.6096 | 1856.1881 | 1850.9001 |
| 4.1504 | 1871.7168 | 1848.7162 | 1843.4894 |
| 4.1614 | 1875.3609 | 1841.2460 | 1836.0788 |
| 4.1724 | 1880.3997 | 1833.7775 | 1828.6681 |
| 4.1834 | 1846.9735 | 1826.3106 | 1821.2574 |
| 4.1944 | 1850.1898 | 1818.8454 | 1813.8467 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 7 Etosha22 RIP 0-1cm S1 heat 550C | 2.0054 | 29.9894 | 0.0110 | 12/4/2023 3:02:08 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.0380 | 680.23 | 0.1299 | 43.31454 | 66.05 |
| 2.6322 | 522.71 | 0.3897 | 33.53720 | 50.76 |
| 5.2841 | 131.04 | 0.1732 | 16.71068 | 12.72 |
| 8.7011 | 1029.85 | 0.1948 | 10.15447 | 100.00 |
| 10.5106 | 50.59 | 0.3464 | 8.40998 | 4.91 |
| 15.8432 | 634.07 | 0.0866 | 5.58925 | 61.57 |
| 17.6463 | 35.84 | 0.2598 | 5.02200 | 3.48 |
| 18.3416 | 43.50 | 0.2598 | 4.83314 | 4.22 |
| 19.6974 | 32.37 | 0.6061 | 4.50343 | 3.14 |
| 26.0649 | 358.12 | 0.1299 | 3.41592 | 34.77 |
| 27.4508 | 74.51 | 0.4330 | 3.24652 | 7.24 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 01-076-8337 | 29 | Potassium Sodium Magnesium Manganese Aluminum Iron Titanium Fluoride Aluminum Silicate Hydroxide | ( K0.84 Na0.03 ) ( Fe0.6 Mg0.33 Mn0.01 ) ( Fe0.39 Al0.27 Mg0.28 Ti0.06 )2 ( ( Si2.71 Al1.29 ) O10.25 ) ( O H )1.68 F0.07 | Biotite-1M | 35 |
| * | 01-083-1730 | 60 | Sodium Aluminum Silicate Hydrate | Na14.96 Al15.36 Si32.64 O96 ( H2 O )16 | Analcime | 32 |
| * | 04-025-4215 | 48 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 16 |
| * | 04-015-2963 | 29 | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate | Mg Al Si4 O10 ( O H ) ( H2 O )4 | Palygorskite-M | 17 |

Anchor Scan Parameters

Dataset Name	7 Etosha22 RIP 0-1cm S1 heat 550C

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\7 Etosha22 RIP 0-1cm S1 heat 550C.xrdml

Sample Identification	7 Etosha22 RIP 0-1cm S1 heat 550C

Measurement Start Date/Time	12/4/2023 3:02:08 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes