7 Etosha 22 RIP 0-1 cm S1 GLYCOLATED

Graphics

Graphics

Graphics

Quantitative Results

Phase Potassium Iron Magnesium Aluminum Silicate Hydroxide

Weight fraction/ %	7.0

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	22.0

Phase Sodium Magnesium Silicon Oxide Hydrate

Weight fraction/ %	9.0

Phase Magnesium Aluminum Iron Silicate Hydroxide Hydrate

Weight fraction/ %	6.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	53.0

Phase Magnesium Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	3.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Potassium Iron Magnesium Aluminum Silicate Hydroxide | Sodium Aluminum Silicate Hydrate | Sodium Magnesium Silicon Oxide Hydrate | Magnesium Aluminum Iron Silicate Hydroxide Hydrate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Magnesium Silicon Oxide Hydroxide Hydrate |
| --- | --- | --- | --- | --- | --- | --- |
| 7 Etosha22 RIP 0-1cm S1 glycolated | 7.0 | 22.0 | 9.0 | 6.0 | 53.0 | 3.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 5425.0000 | 5417.8361 | 5425.0000 |
| 2.0164 | 5318.1106 | 5387.3844 | 5387.3844 |
| 2.0274 | 5325.0088 | 5349.7687 | 5349.7687 |
| 2.0384 | 5239.9897 | 5312.1531 | 5312.1531 |
| 2.0494 | 5089.8338 | 5274.5375 | 5274.5375 |
| 2.0604 | 5214.9941 | 5236.9219 | 5236.9219 |
| 2.0714 | 5108.4425 | 5199.3062 | 5199.3062 |
| 2.0824 | 5116.2370 | 5161.6906 | 5161.6906 |
| 2.0934 | 5126.9223 | 5124.0750 | 5124.0750 |
| 2.1044 | 5005.3407 | 5086.4594 | 5086.4594 |
| 2.1154 | 4982.0442 | 5048.8437 | 5048.8437 |
| 2.1264 | 4921.6809 | 5011.2281 | 5011.2281 |
| 2.1374 | 4991.1799 | 4973.6125 | 4973.6125 |
| 2.1484 | 4998.4794 | 4935.9969 | 4935.9969 |
| 2.1594 | 4969.3382 | 4898.3812 | 4898.3812 |
| 2.1704 | 4812.0221 | 4860.7656 | 4860.7656 |
| 2.1814 | 4790.9833 | 4823.1500 | 4823.1500 |
| 2.1924 | 4789.5674 | 4787.6864 | 4785.5344 |
| 2.2034 | 4774.3097 | 4759.2183 | 4759.2183 |
| 2.2144 | 4776.4194 | 4732.9022 | 4732.9022 |
| 2.2254 | 4718.8043 | 4706.5862 | 4706.5862 |
| 2.2364 | 4706.6770 | 4680.2701 | 4680.2701 |
| 2.2474 | 4711.6273 | 4653.9541 | 4653.9541 |
| 2.2584 | 4713.0344 | 4627.6380 | 4627.6380 |
| 2.2694 | 4612.8112 | 4601.3219 | 4601.3219 |
| 2.2804 | 4547.6254 | 4575.0059 | 4575.0059 |
| 2.2914 | 4507.6716 | 4548.6898 | 4548.6898 |
| 2.3024 | 4473.9292 | 4522.3738 | 4522.3738 |
| 2.3134 | 4487.4159 | 4496.0577 | 4496.0577 |
| 2.3244 | 4436.6731 | 4469.7416 | 4469.7416 |
| 2.3354 | 4428.5428 | 4443.4256 | 4443.4256 |
| 2.3464 | 4425.4218 | 4417.1095 | 4417.1095 |
| 2.3574 | 4410.4445 | 4390.7935 | 4390.7935 |
| 2.3684 | 4415.3200 | 4364.4774 | 4364.4774 |
| 2.3794 | 4299.0157 | 4338.6017 | 4338.1614 |
| 2.3904 | 4284.6377 | 4314.1572 | 4314.1572 |
| 2.4014 | 4319.5044 | 4290.1530 | 4290.1530 |
| 2.4124 | 4318.0831 | 4266.1488 | 4266.1488 |
| 2.4234 | 4310.6765 | 4242.1447 | 4242.1447 |
| 2.4344 | 4287.5693 | 4218.1405 | 4218.1405 |
| 2.4454 | 4165.8958 | 4194.1363 | 4194.1363 |
| 2.4564 | 4119.2989 | 4170.1322 | 4170.1322 |
| 2.4674 | 4167.3245 | 4146.1280 | 4146.1280 |
| 2.4784 | 4086.0954 | 4122.1238 | 4122.1238 |
| 2.4894 | 4043.9381 | 4098.1196 | 4098.1196 |
| 2.5004 | 4049.8982 | 4074.1155 | 4074.1155 |
| 2.5114 | 4059.0964 | 4050.1113 | 4050.1113 |
| 2.5224 | 4092.2429 | 4026.1071 | 4026.1071 |
| 2.5334 | 4044.7227 | 4002.1030 | 4002.1030 |
| 2.5444 | 4017.2384 | 3978.0988 | 3978.0988 |
| 2.5554 | 3907.2350 | 3954.0946 | 3954.0946 |
| 2.5664 | 3905.4602 | 3931.3250 | 3930.0905 |
| 2.5774 | 3943.5261 | 3912.5687 | 3912.5687 |
| 2.5884 | 3935.1372 | 3895.0470 | 3895.0470 |
| 2.5994 | 3928.6814 | 3877.5253 | 3877.5253 |
| 2.6104 | 3919.5639 | 3860.0036 | 3860.0036 |
| 2.6214 | 3843.7286 | 3842.4819 | 3842.4819 |
| 2.6324 | 3806.0959 | 3824.9602 | 3824.9602 |
| 2.6434 | 3838.2183 | 3807.4384 | 3807.4384 |
| 2.6544 | 3849.8245 | 3789.9167 | 3789.9167 |
| 2.6654 | 3713.3068 | 3772.3950 | 3772.3950 |
| 2.6764 | 3692.7409 | 3754.8733 | 3754.8733 |
| 2.6874 | 3737.8161 | 3737.9478 | 3737.3516 |
| 2.6984 | 3672.3407 | 3720.9339 | 3719.8299 |
| 2.7094 | 3657.8663 | 3703.5240 | 3702.3081 |
| 2.7204 | 3721.5167 | 3686.0127 | 3684.7864 |
| 2.7314 | 3672.1032 | 3668.5015 | 3667.2647 |
| 2.7424 | 3708.8805 | 3650.9905 | 3649.7430 |
| 2.7534 | 3586.2733 | 3633.7730 | 3632.2213 |
| 2.7644 | 3593.9233 | 3617.5094 | 3616.2401 |
| 2.7754 | 3581.0718 | 3601.5394 | 3600.2589 |
| 2.7864 | 3576.2547 | 3585.5695 | 3584.2777 |
| 2.7974 | 3483.9646 | 3569.5997 | 3568.2966 |
| 2.8084 | 3456.7468 | 3553.6301 | 3552.3154 |
| 2.8194 | 3514.1200 | 3537.6607 | 3536.3342 |
| 2.8304 | 3511.7035 | 3521.6914 | 3520.3530 |
| 2.8414 | 3398.9056 | 3505.7222 | 3504.3718 |
| 2.8524 | 3537.6937 | 3489.7533 | 3488.3907 |
| 2.8634 | 3527.7847 | 3473.7845 | 3472.4095 |
| 2.8744 | 3399.7999 | 3457.8158 | 3456.4283 |
| 2.8854 | 3449.0974 | 3441.8474 | 3440.4471 |
| 2.8964 | 3389.2699 | 3425.8791 | 3424.4659 |
| 2.9074 | 3427.9371 | 3409.9110 | 3408.4848 |
| 2.9184 | 3419.2340 | 3393.9431 | 3392.5036 |
| 2.9294 | 3379.7611 | 3377.9753 | 3376.5224 |
| 2.9404 | 3316.3107 | 3362.2283 | 3360.5412 |
| 2.9514 | 3384.0344 | 3347.1982 | 3345.7179 |
| 2.9624 | 3331.3953 | 3332.3889 | 3330.8945 |
| 2.9734 | 3288.5497 | 3317.5797 | 3316.0711 |
| 2.9844 | 3347.0560 | 3302.7708 | 3301.2478 |
| 2.9954 | 3309.3186 | 3287.9621 | 3286.4244 |
| 3.0064 | 3298.4926 | 3273.1536 | 3271.6011 |
| 3.0174 | 3203.1003 | 3258.3453 | 3256.7777 |
| 3.0284 | 3242.0074 | 3243.5372 | 3241.9543 |
| 3.0394 | 3271.2232 | 3228.7293 | 3227.1310 |
| 3.0504 | 3251.2409 | 3213.9217 | 3212.3076 |
| 3.0614 | 3172.1003 | 3199.1143 | 3197.4843 |
| 3.0724 | 3176.6505 | 3184.3071 | 3182.6609 |
| 3.0834 | 3192.1386 | 3169.5002 | 3167.8375 |
| 3.0944 | 3092.1372 | 3154.6935 | 3153.0142 |
| 3.1054 | 3051.2635 | 3139.8871 | 3138.1908 |
| 3.1164 | 3138.8963 | 3125.0809 | 3123.3675 |
| 3.1274 | 3126.5074 | 3110.6684 | 3108.5441 |
| 3.1384 | 3108.0516 | 3097.5345 | 3095.7858 |
| 3.1494 | 3069.9744 | 3084.7943 | 3083.0276 |
| 3.1604 | 3072.4498 | 3072.0543 | 3070.2694 |
| 3.1714 | 2999.7709 | 3059.3146 | 3057.5111 |
| 3.1824 | 3062.2183 | 3046.5753 | 3044.7529 |
| 3.1934 | 3035.0088 | 3033.8362 | 3031.9946 |
| 3.2044 | 2963.3864 | 3021.0974 | 3019.2364 |
| 3.2154 | 2934.1455 | 3008.3589 | 3006.4781 |
| 3.2264 | 2991.1711 | 2995.6207 | 2993.7199 |
| 3.2374 | 2976.1042 | 2982.8829 | 2980.9616 |
| 3.2484 | 2959.0556 | 2970.1454 | 2968.2034 |
| 3.2594 | 2975.4897 | 2957.4082 | 2955.4451 |
| 3.2704 | 3020.5865 | 2944.6714 | 2942.6869 |
| 3.2814 | 2952.3038 | 2931.9349 | 2929.9287 |
| 3.2924 | 2864.9425 | 2919.1988 | 2917.1704 |
| 3.3034 | 2869.5497 | 2906.4631 | 2904.4122 |
| 3.3144 | 2895.3702 | 2894.2037 | 2891.6539 |
| 3.3254 | 2930.7493 | 2883.4923 | 2881.3953 |
| 3.3364 | 2888.2527 | 2873.2574 | 2871.1367 |
| 3.3474 | 2837.0010 | 2863.0228 | 2860.8781 |
| 3.3584 | 2833.9528 | 2852.7886 | 2850.6195 |
| 3.3694 | 2817.3255 | 2842.5549 | 2840.3608 |
| 3.3804 | 2821.1642 | 2832.3216 | 2830.1022 |
| 3.3914 | 2802.5310 | 2822.0888 | 2819.8436 |
| 3.4024 | 2789.5851 | 2811.8563 | 2809.5850 |
| 3.4134 | 2751.7001 | 2801.6244 | 2799.3264 |
| 3.4244 | 2706.8024 | 2791.3929 | 2789.0678 |
| 3.4354 | 2793.0669 | 2781.1619 | 2778.8092 |
| 3.4464 | 2780.5644 | 2770.9314 | 2768.5505 |
| 3.4574 | 2718.6844 | 2760.7014 | 2758.2919 |
| 3.4684 | 2746.1785 | 2750.4719 | 2748.0333 |
| 3.4794 | 2713.9459 | 2740.2430 | 2737.7747 |
| 3.4904 | 2745.6549 | 2730.0146 | 2727.5161 |
| 3.5014 | 2752.1514 | 2720.0464 | 2717.2575 |
| 3.5124 | 2675.0319 | 2710.9226 | 2708.3620 |
| 3.5234 | 2661.0118 | 2702.0591 | 2699.4665 |
| 3.5344 | 2661.6239 | 2693.1961 | 2690.5711 |
| 3.5454 | 2637.3776 | 2684.3338 | 2681.6756 |
| 3.5564 | 2705.2360 | 2675.4721 | 2672.7801 |
| 3.5674 | 2611.5113 | 2666.6111 | 2663.8847 |
| 3.5784 | 2616.2149 | 2657.7507 | 2654.9892 |
| 3.5894 | 2618.6814 | 2648.8910 | 2646.0937 |
| 3.6004 | 2666.6254 | 2640.0320 | 2637.1983 |
| 3.6114 | 2671.4661 | 2631.1737 | 2628.3028 |
| 3.6224 | 2622.2065 | 2622.3161 | 2619.4073 |
| 3.6334 | 2732.2232 | 2613.4593 | 2610.5119 |
| 3.6444 | 2624.3185 | 2604.6033 | 2601.6164 |
| 3.6554 | 2580.1268 | 2595.7480 | 2592.7209 |
| 3.6664 | 2584.7035 | 2586.8936 | 2583.8255 |
| 3.6774 | 2574.7129 | 2578.0400 | 2574.9300 |
| 3.6884 | 2572.1195 | 2570.9814 | 2566.0345 |
| 3.6994 | 2519.3235 | 2565.3678 | 2562.1714 |
| 3.7104 | 2628.8545 | 2561.5492 | 2558.3082 |
| 3.7214 | 2574.0295 | 2557.7315 | 2554.4451 |
| 3.7324 | 2552.1952 | 2553.9148 | 2550.5819 |
| 3.7434 | 2507.6686 | 2550.0990 | 2546.7187 |
| 3.7544 | 2551.7596 | 2546.2843 | 2542.8556 |
| 3.7654 | 2546.2675 | 2542.4706 | 2538.9924 |
| 3.7764 | 2514.6765 | 2538.6580 | 2535.1292 |
| 3.7874 | 2544.7257 | 2534.8466 | 2531.2661 |
| 3.7984 | 2571.0792 | 2531.0362 | 2527.4029 |
| 3.8094 | 2594.4563 | 2527.2270 | 2523.5398 |
| 3.8204 | 2620.3938 | 2523.4191 | 2519.6766 |
| 3.8314 | 2532.1770 | 2519.6124 | 2515.8134 |
| 3.8424 | 2582.1062 | 2515.8069 | 2511.9503 |
| 3.8534 | 2541.1858 | 2512.0028 | 2508.0871 |
| 3.8644 | 2452.1854 | 2508.2001 | 2504.2239 |
| 3.8754 | 2558.5998 | 2504.3065 | 2500.3608 |
| 3.8864 | 2529.1903 | 2500.3400 | 2496.2388 |
| 3.8974 | 2573.4031 | 2496.2828 | 2492.1168 |
| 3.9084 | 2548.3648 | 2492.2272 | 2487.9949 |
| 3.9194 | 2474.5871 | 2488.1731 | 2483.8729 |
| 3.9304 | 2564.5846 | 2484.1207 | 2479.7509 |
| 3.9414 | 2594.6942 | 2480.0699 | 2475.6289 |
| 3.9524 | 2577.6445 | 2476.0209 | 2471.5070 |
| 3.9634 | 2534.2586 | 2471.9737 | 2467.3850 |
| 3.9744 | 2566.6047 | 2467.9284 | 2463.2630 |
| 3.9854 | 2585.6725 | 2463.8850 | 2459.1410 |
| 3.9964 | 2515.5728 | 2459.8437 | 2455.0190 |
| 4.0074 | 2524.5546 | 2455.8043 | 2450.8971 |
| 4.0184 | 2517.3053 | 2451.7671 | 2446.7751 |
| 4.0294 | 2485.5861 | 2447.7322 | 2442.6531 |
| 4.0404 | 2544.5939 | 2443.6995 | 2438.5311 |
| 4.0514 | 2544.1829 | 2439.6692 | 2434.4092 |
| 4.0624 | 2609.3142 | 2435.5485 | 2430.2872 |
| 4.0734 | 2529.6705 | 2431.3556 | 2425.9049 |
| 4.0844 | 2435.4779 | 2427.0726 | 2421.5227 |
| 4.0954 | 2610.1829 | 2422.7924 | 2417.1404 |
| 4.1064 | 2645.9307 | 2418.5149 | 2412.7581 |
| 4.1174 | 2557.7728 | 2414.2404 | 2408.3758 |
| 4.1284 | 2494.6991 | 2409.9689 | 2403.9936 |
| 4.1394 | 2530.9902 | 2405.7006 | 2399.6113 |
| 4.1504 | 2575.7611 | 2401.4355 | 2395.2290 |
| 4.1614 | 2596.9076 | 2397.1739 | 2390.8468 |
| 4.1724 | 2614.8933 | 2392.9158 | 2386.4645 |
| 4.1834 | 2615.4690 | 2388.6614 | 2382.0822 |
| 4.1944 | 2629.3643 | 2384.4107 | 2377.7000 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 7 Etosha22 RIP 0-1cm S1 glycolated | 2.0054 | 29.9894 | 0.0110 | 12/5/2023 7:43:31 AM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 5.2797 | 847.34 | 0.2598 | 16.72467 | 58.79 |
| 6.9665 | 1441.25 | 0.1732 | 12.67850 | 100.00 |
| 8.7667 | 807.78 | 0.1515 | 10.07854 | 56.05 |
| 15.7728 | 1232.07 | 0.1191 | 5.61405 | 85.49 |
| 17.6590 | 66.95 | 0.2165 | 5.01840 | 4.65 |
| 18.2234 | 187.65 | 0.1082 | 4.86422 | 13.02 |
| 19.8239 | 55.76 | 0.4330 | 4.47498 | 3.87 |
| 23.4156 | 45.58 | 0.2598 | 3.79606 | 3.16 |
| 24.2385 | 48.93 | 0.2598 | 3.66901 | 3.39 |
| 25.9162 | 1374.96 | 0.1191 | 3.43517 | 95.40 |
| 26.7692 | 254.07 | 0.1948 | 3.32762 | 17.63 |
| 27.5421 | 75.51 | 0.1732 | 3.23597 | 5.24 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 00-042-1437 | 50 | Potassium Iron Magnesium Aluminum Silicate Hydroxide | K ( Mg , Fe )3 ( Al , Fe ) Si3 O10 ( O H , F )2 | Phlogopite-1M, Fe+2-bearing | 7 |
| * | 01-072-4625 | 61 | Sodium Aluminum Silicate Hydrate | Na Al ( Si2 O6 ) ( H2 O ) | Analcime | 22 |
| * | 01-082-8023 | 26 | Sodium Magnesium Silicon Oxide Hydrate | Na2 Mg3 ( Si6 O16 ) ( H2 O )7 | Loughlinite | 9 |
| * | 01-076-7133 | 14 | Magnesium Aluminum Iron Silicate Hydroxide Hydrate | ( Mg2.09 Al1.92 Fe0.11 ) ( ( Si7.8 Al0.2 ) ( H2 O )4 O20 ) ( O H )2 ( H2 O )4.48 | Palygorskite-M | 6 |
| * | 04-025-4215 | 6 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 53 |
| * | 01-080-5781 | 13 | Magnesium Silicon Oxide Hydroxide Hydrate | Mg8 ( Si12 O30 ( O H )4 ( H2 O )3.92 ) ( H2 O )7.72 | Sepiolite | 3 |

Anchor Scan Parameters

Dataset Name	7 Etosha22 RIP 0-1cm S1 glycolated

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\7 Etosha22 RIP 0-1cm S1 glycolated.xrdml

Sample Identification	7 Etosha22 RIP 0-1cm S1 glycolated

Measurement Start Date/Time	12/5/2023 7:43:31 AM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes