7 Etosha 22 RIP 0-1 cm S1 REGULAR

Graphics

Graphics

Graphics

Quantitative Results

Phase Potassium Iron Magnesium Aluminum Silicate Hydroxide

Weight fraction/ %	6.0

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	21.0

Phase Potassium Sodium Magnesium Manganese Aluminum Iron Titanium Fluoride Aluminum Silicate Hydroxide

Weight fraction/ %	10.0

Phase Magnesium Aluminum Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	4.0

Phase Sodium Magnesium Silicon Oxide Hydrate

Weight fraction/ %	14.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	45.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Potassium Iron Magnesium Aluminum Silicate Hydroxide | Sodium Aluminum Silicate Hydrate | Potassium Sodium Magnesium Manganese Aluminum Iron Titanium Fluoride Aluminum Silicate Hydroxide | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate | Sodium Magnesium Silicon Oxide Hydrate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide |
| --- | --- | --- | --- | --- | --- | --- |
| 7 Etosha22 RIP 0-1cm S1 | 6.0 | 21.0 | 10.0 | 4.0 | 14.0 | 45.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 5037.0000 | 5020.5398 | 5037.0000 |
| 2.0164 | 4916.7498 | 5001.3469 | 5001.3469 |
| 2.0274 | 4972.5015 | 4965.6937 | 4965.6937 |
| 2.0384 | 4795.2168 | 4930.0406 | 4930.0406 |
| 2.0494 | 4823.4110 | 4894.3875 | 4894.3875 |
| 2.0604 | 4754.1844 | 4858.7343 | 4858.7343 |
| 2.0714 | 4754.8614 | 4823.0812 | 4823.0812 |
| 2.0824 | 4718.0197 | 4787.4280 | 4787.4280 |
| 2.0934 | 4628.7158 | 4751.7749 | 4751.7749 |
| 2.1044 | 4765.6283 | 4716.1218 | 4716.1218 |
| 2.1154 | 4638.3019 | 4680.4686 | 4680.4686 |
| 2.1264 | 4641.6893 | 4644.8155 | 4644.8155 |
| 2.1374 | 4473.7847 | 4609.1624 | 4609.1624 |
| 2.1484 | 4522.7468 | 4573.5092 | 4573.5092 |
| 2.1594 | 4550.7699 | 4537.8561 | 4537.8561 |
| 2.1704 | 4439.3687 | 4502.2030 | 4502.2030 |
| 2.1814 | 4440.2134 | 4466.5498 | 4466.5498 |
| 2.1924 | 4424.8810 | 4435.9220 | 4430.8967 |
| 2.2034 | 4398.0266 | 4406.1284 | 4406.1284 |
| 2.2144 | 4454.2576 | 4381.3602 | 4381.3602 |
| 2.2254 | 4392.4513 | 4356.5920 | 4356.5920 |
| 2.2364 | 4319.7758 | 4331.8237 | 4331.8237 |
| 2.2474 | 4344.4592 | 4307.0555 | 4307.0555 |
| 2.2584 | 4328.0172 | 4282.2873 | 4282.2873 |
| 2.2694 | 4302.6844 | 4257.5190 | 4257.5190 |
| 2.2804 | 4304.4233 | 4232.7508 | 4232.7508 |
| 2.2914 | 4233.9282 | 4207.9826 | 4207.9826 |
| 2.3024 | 4194.4513 | 4183.2143 | 4183.2143 |
| 2.3134 | 4129.6431 | 4158.4461 | 4158.4461 |
| 2.3244 | 4103.3663 | 4133.6779 | 4133.6779 |
| 2.3354 | 4099.7935 | 4108.9096 | 4108.9096 |
| 2.3464 | 4098.0934 | 4084.1414 | 4084.1414 |
| 2.3574 | 4061.9410 | 4059.3731 | 4059.3731 |
| 2.3684 | 4075.6165 | 4034.6049 | 4034.6049 |
| 2.3794 | 4040.7050 | 4012.2301 | 4009.8367 |
| 2.3904 | 3917.3471 | 3991.2913 | 3988.7948 |
| 2.4014 | 3930.1504 | 3971.0013 | 3967.7528 |
| 2.4124 | 3945.3766 | 3949.9744 | 3946.7109 |
| 2.4234 | 3918.1504 | 3928.9477 | 3925.6690 |
| 2.4344 | 3890.7861 | 3907.9210 | 3904.6271 |
| 2.4454 | 3931.5418 | 3886.8945 | 3883.5852 |
| 2.4564 | 3870.5437 | 3865.8681 | 3862.5432 |
| 2.4674 | 3837.7788 | 3844.8418 | 3841.5013 |
| 2.4784 | 3859.9430 | 3823.8156 | 3820.4594 |
| 2.4894 | 3797.8889 | 3802.7895 | 3799.4175 |
| 2.5004 | 3742.1283 | 3781.7635 | 3778.3756 |
| 2.5114 | 3742.3923 | 3760.7377 | 3757.3336 |
| 2.5224 | 3753.0875 | 3739.7119 | 3736.2917 |
| 2.5334 | 3746.0206 | 3718.6863 | 3715.2498 |
| 2.5444 | 3680.9897 | 3697.6607 | 3694.2079 |
| 2.5554 | 3706.0698 | 3676.6353 | 3673.1660 |
| 2.5664 | 3644.7050 | 3658.3393 | 3652.1240 |
| 2.5774 | 3628.4612 | 3640.4965 | 3636.9937 |
| 2.5884 | 3594.3717 | 3625.3830 | 3621.8633 |
| 2.5994 | 3549.7257 | 3610.2696 | 3606.7330 |
| 2.6104 | 3585.5885 | 3595.1564 | 3591.6026 |
| 2.6214 | 3597.7404 | 3580.0433 | 3576.4723 |
| 2.6324 | 3596.1018 | 3564.9303 | 3561.3419 |
| 2.6434 | 3611.9705 | 3549.8175 | 3546.2116 |
| 2.6544 | 3528.8038 | 3534.7048 | 3531.0812 |
| 2.6654 | 3586.4454 | 3519.5922 | 3515.9509 |
| 2.6764 | 3526.7802 | 3504.4797 | 3500.8205 |
| 2.6874 | 3556.2016 | 3489.3674 | 3485.6902 |
| 2.6984 | 3523.8938 | 3474.2552 | 3470.5598 |
| 2.7094 | 3475.9616 | 3459.1431 | 3455.4295 |
| 2.7204 | 3418.2660 | 3444.0312 | 3440.2991 |
| 2.7314 | 3448.9941 | 3428.9194 | 3425.1688 |
| 2.7424 | 3449.9415 | 3413.8078 | 3410.0384 |
| 2.7534 | 3419.5831 | 3398.6125 | 3394.9081 |
| 2.7644 | 3425.0251 | 3383.4035 | 3379.5963 |
| 2.7754 | 3308.2684 | 3368.1109 | 3364.2846 |
| 2.7864 | 3382.3751 | 3352.8184 | 3348.9728 |
| 2.7974 | 3398.6549 | 3337.5261 | 3333.6611 |
| 2.8084 | 3320.0423 | 3322.2339 | 3318.3493 |
| 2.8194 | 3260.9754 | 3306.9419 | 3303.0376 |
| 2.8304 | 3241.2507 | 3291.6500 | 3287.7259 |
| 2.8414 | 3270.8260 | 3276.3583 | 3272.4141 |
| 2.8524 | 3298.5531 | 3261.0667 | 3257.1024 |
| 2.8634 | 3267.4041 | 3245.7753 | 3241.7906 |
| 2.8744 | 3211.6244 | 3230.4840 | 3226.4789 |
| 2.8854 | 3214.9164 | 3215.1929 | 3211.1671 |
| 2.8964 | 3087.5664 | 3199.9020 | 3195.8554 |
| 2.9074 | 3155.1819 | 3184.6112 | 3180.5437 |
| 2.9184 | 3055.2050 | 3169.3206 | 3165.2319 |
| 2.9294 | 3208.7286 | 3154.0301 | 3149.9202 |
| 2.9404 | 3140.6421 | 3138.7398 | 3134.6084 |
| 2.9514 | 3134.4828 | 3123.4497 | 3119.2967 |
| 2.9624 | 3158.1681 | 3108.1598 | 3103.9850 |
| 2.9734 | 3139.3284 | 3092.8700 | 3088.6732 |
| 2.9844 | 3058.1647 | 3077.5804 | 3073.3615 |
| 2.9954 | 3104.3894 | 3062.2910 | 3058.0497 |
| 3.0064 | 3067.0093 | 3047.0017 | 3042.7380 |
| 3.0174 | 3027.2930 | 3031.7126 | 3027.4262 |
| 3.0284 | 3094.6932 | 3016.4237 | 3012.1145 |
| 3.0394 | 3031.5271 | 3001.1350 | 2996.8028 |
| 3.0504 | 3133.2114 | 2985.8465 | 2981.4910 |
| 3.0614 | 3014.7050 | 2970.5582 | 2966.1793 |
| 3.0724 | 2952.4971 | 2955.2700 | 2950.8675 |
| 3.0834 | 2958.6391 | 2939.9821 | 2935.5558 |
| 3.0944 | 2875.8274 | 2924.6943 | 2920.2440 |
| 3.1054 | 2929.3343 | 2909.4067 | 2904.9323 |
| 3.1164 | 2914.1032 | 2894.1194 | 2889.6206 |
| 3.1274 | 2888.5103 | 2881.7377 | 2874.3088 |
| 3.1384 | 2830.1588 | 2869.8386 | 2865.2905 |
| 3.1494 | 2820.8093 | 2860.8453 | 2856.2721 |
| 3.1604 | 2871.0678 | 2851.8521 | 2847.2538 |
| 3.1714 | 2877.3658 | 2842.8591 | 2838.2354 |
| 3.1824 | 2861.4366 | 2833.8664 | 2829.2171 |
| 3.1934 | 2816.5133 | 2824.8739 | 2820.1988 |
| 3.2044 | 2800.4656 | 2815.8816 | 2811.1804 |
| 3.2154 | 2869.6234 | 2806.8895 | 2802.1621 |
| 3.2264 | 2805.6548 | 2797.8976 | 2793.1437 |
| 3.2374 | 2727.9616 | 2788.9059 | 2784.1254 |
| 3.2484 | 2746.8334 | 2779.9145 | 2775.1070 |
| 3.2594 | 2794.7847 | 2770.9233 | 2766.0887 |
| 3.2704 | 2803.5388 | 2761.9323 | 2757.0703 |
| 3.2814 | 2789.9587 | 2752.9416 | 2748.0520 |
| 3.2924 | 2749.1991 | 2743.9511 | 2739.0337 |
| 3.3034 | 2790.7227 | 2734.9608 | 2730.0153 |
| 3.3144 | 2757.1421 | 2725.8405 | 2720.9970 |
| 3.3254 | 2677.8997 | 2716.6987 | 2711.6963 |
| 3.3364 | 2710.2075 | 2707.4269 | 2702.3957 |
| 3.3474 | 2697.5437 | 2698.1553 | 2693.0950 |
| 3.3584 | 2647.3702 | 2688.8840 | 2683.7944 |
| 3.3694 | 2663.4877 | 2679.6129 | 2674.4938 |
| 3.3804 | 2667.4449 | 2670.3421 | 2665.1931 |
| 3.3914 | 2647.9646 | 2661.0715 | 2655.8925 |
| 3.4024 | 2630.6588 | 2651.8012 | 2646.5918 |
| 3.4134 | 2614.1209 | 2642.5312 | 2637.2912 |
| 3.4244 | 2606.0723 | 2633.2615 | 2627.9906 |
| 3.4354 | 2655.4140 | 2623.9920 | 2618.6899 |
| 3.4464 | 2677.7974 | 2614.7228 | 2609.3893 |
| 3.4574 | 2613.9823 | 2605.4539 | 2600.0887 |
| 3.4684 | 2566.6711 | 2596.1852 | 2590.7880 |
| 3.4794 | 2612.7011 | 2586.9169 | 2581.4874 |
| 3.4904 | 2583.9823 | 2577.6488 | 2572.1867 |
| 3.5014 | 2565.4169 | 2568.3811 | 2562.8861 |
| 3.5124 | 2619.5551 | 2559.1136 | 2553.5855 |
| 3.5234 | 2564.0295 | 2549.8464 | 2544.2848 |
| 3.5344 | 2593.7611 | 2540.5796 | 2534.9842 |
| 3.5454 | 2555.1327 | 2531.3130 | 2525.6835 |
| 3.5564 | 2560.0546 | 2522.0468 | 2516.3829 |
| 3.5674 | 2521.8082 | 2512.7808 | 2507.0823 |
| 3.5784 | 2539.8506 | 2503.5152 | 2497.7816 |
| 3.5894 | 2419.3451 | 2494.2499 | 2488.4810 |
| 3.6004 | 2410.5059 | 2484.9850 | 2479.1803 |
| 3.6114 | 2441.2458 | 2475.7203 | 2469.8797 |
| 3.6224 | 2449.4204 | 2466.4561 | 2460.5791 |
| 3.6334 | 2377.1022 | 2457.1921 | 2451.2784 |
| 3.6444 | 2449.1249 | 2447.9285 | 2441.9778 |
| 3.6554 | 2456.8761 | 2438.6652 | 2432.6771 |
| 3.6664 | 2412.2025 | 2429.4023 | 2423.3765 |
| 3.6774 | 2349.4326 | 2420.1398 | 2414.0759 |
| 3.6884 | 2401.7567 | 2412.3668 | 2404.7752 |
| 3.6994 | 2444.8201 | 2404.8415 | 2398.7003 |
| 3.7104 | 2441.7591 | 2398.8058 | 2392.6254 |
| 3.7214 | 2361.1858 | 2392.7705 | 2386.5505 |
| 3.7324 | 2470.2119 | 2386.7355 | 2380.4756 |
| 3.7434 | 2339.5860 | 2380.7009 | 2374.4007 |
| 3.7544 | 2434.0620 | 2374.6667 | 2368.3258 |
| 3.7654 | 2458.3314 | 2368.6330 | 2362.2509 |
| 3.7764 | 2323.9174 | 2362.5996 | 2356.1760 |
| 3.7874 | 2337.8496 | 2356.5666 | 2350.1011 |
| 3.7984 | 2275.3235 | 2350.5340 | 2344.0262 |
| 3.8094 | 2369.4405 | 2344.5019 | 2337.9513 |
| 3.8204 | 2395.0944 | 2338.4701 | 2331.8764 |
| 3.8314 | 2330.9754 | 2332.4388 | 2325.8015 |
| 3.8424 | 2368.8466 | 2326.4080 | 2319.7266 |
| 3.8534 | 2213.9941 | 2320.3775 | 2313.6517 |
| 3.8644 | 2355.7615 | 2314.3475 | 2307.5768 |
| 3.8754 | 2321.3048 | 2308.9959 | 2301.5019 |
| 3.8864 | 2249.3098 | 2303.7572 | 2296.8952 |
| 3.8974 | 2315.2655 | 2299.1968 | 2292.2886 |
| 3.9084 | 2374.6573 | 2294.6369 | 2287.6819 |
| 3.9194 | 2232.8909 | 2290.0775 | 2283.0753 |
| 3.9304 | 2240.1878 | 2285.5186 | 2278.4686 |
| 3.9414 | 2302.3716 | 2280.9602 | 2273.8620 |
| 3.9524 | 2222.5310 | 2276.4022 | 2269.2554 |
| 3.9634 | 2272.9390 | 2271.8448 | 2264.6487 |
| 3.9744 | 2282.2026 | 2267.2878 | 2260.0421 |
| 3.9854 | 2305.1239 | 2262.7314 | 2255.4354 |
| 3.9964 | 2304.4621 | 2258.1755 | 2250.8288 |
| 4.0074 | 2243.4827 | 2253.6201 | 2246.2221 |
| 4.0184 | 2161.9410 | 2249.0653 | 2241.6155 |
| 4.0294 | 2210.7532 | 2244.5110 | 2237.0088 |
| 4.0404 | 2184.2031 | 2239.9573 | 2232.4022 |
| 4.0514 | 2214.8820 | 2235.4041 | 2227.7955 |
| 4.0624 | 2261.7748 | 2230.8515 | 2223.1889 |
| 4.0734 | 2238.8210 | 2226.2995 | 2218.5823 |
| 4.0844 | 2172.0443 | 2221.7480 | 2213.9756 |
| 4.0954 | 2198.7119 | 2217.1972 | 2209.3690 |
| 4.1064 | 2192.7969 | 2212.6469 | 2204.7623 |
| 4.1174 | 2168.4749 | 2208.0973 | 2200.1557 |
| 4.1284 | 2198.9774 | 2203.5483 | 2195.5490 |
| 4.1394 | 2216.3029 | 2198.9999 | 2190.9424 |
| 4.1504 | 2224.4941 | 2194.4522 | 2186.3357 |
| 4.1614 | 2203.7276 | 2189.9051 | 2181.7291 |
| 4.1724 | 2164.8717 | 2185.3586 | 2177.1225 |
| 4.1834 | 2122.3363 | 2180.8128 | 2172.5158 |
| 4.1944 | 2126.2163 | 2176.2677 | 2167.9092 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 7 Etosha22 RIP 0-1cm S1 | 2.0054 | 29.9894 | 0.0110 | 12/1/2023 1:49:00 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 7.1411 | 2288.37 | 0.4763 | 12.36878 | 100.00 |
| 8.7557 | 582.73 | 0.1515 | 10.09126 | 25.46 |
| 13.0393 | 26.22 | 0.6927 | 6.78417 | 1.15 |
| 15.7601 | 1017.94 | 0.1082 | 5.61852 | 44.48 |
| 17.6661 | 65.56 | 0.2598 | 5.01641 | 2.87 |
| 18.2265 | 151.58 | 0.1082 | 4.86341 | 6.62 |
| 19.5713 | 76.84 | 0.4330 | 4.53217 | 3.36 |
| 23.5076 | 29.49 | 0.3464 | 3.78142 | 1.29 |
| 24.2156 | 58.84 | 0.1299 | 3.67243 | 2.57 |
| 25.9301 | 1065.52 | 0.0758 | 3.43336 | 46.56 |
| 26.7122 | 197.21 | 0.1732 | 3.33459 | 8.62 |
| 27.4797 | 50.37 | 0.2598 | 3.24317 | 2.20 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 00-042-1437 | 42 | Potassium Iron Magnesium Aluminum Silicate Hydroxide | K ( Mg , Fe )3 ( Al , Fe ) Si3 O10 ( O H , F )2 | Phlogopite-1M, Fe+2-bearing | 6 |
| * | 01-072-4625 | 63 | Sodium Aluminum Silicate Hydrate | Na Al ( Si2 O6 ) ( H2 O ) | Analcime | 21 |
| * | 01-076-8337 | 25 | Potassium Sodium Magnesium Manganese Aluminum Iron Titanium Fluoride Aluminum Silicate Hydroxide | ( K0.84 Na0.03 ) ( Fe0.6 Mg0.33 Mn0.01 ) ( Fe0.39 Al0.27 Mg0.28 Ti0.06 )2 ( ( Si2.71 Al1.29 ) O10.25 ) ( O H )1.68 F0.07 | Biotite-1M | 10 |
| * | 04-015-2963 | 11 | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate | Mg Al Si4 O10 ( O H ) ( H2 O )4 | Palygorskite-M | 4 |
| * | 01-082-8023 | 16 | Sodium Magnesium Silicon Oxide Hydrate | Na2 Mg3 ( Si6 O16 ) ( H2 O )7 | Loughlinite | 14 |
| * | 04-025-4215 | 6 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 45 |

Anchor Scan Parameters

Dataset Name	7 Etosha22 RIP 0-1cm S1

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\7 Etosha22 RIP 0-1cm S1.xrdml

Sample Identification	7 Etosha22 RIP 0-1cm S1

Measurement Start Date/Time	12/1/2023 1:49:00 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes