8 Etosha 22 CRT 0-0.1 cm S1 400 C

Graphics

Graphics

Graphics

Quantitative Results

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	27.0

Phase Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide

Weight fraction/ %	18.0

Phase Potassium Manganese Aluminum Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	16.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	18.0

Phase Magnesium Silicate Hydroxide Hydrate

Weight fraction/ %	20.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Sodium Aluminum Silicate Hydrate | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | Potassium Manganese Aluminum Silicon Oxide Hydroxide Hydrate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Magnesium Silicate Hydroxide Hydrate |
| --- | --- | --- | --- | --- | --- |
| 8 Etosha22 Crt 0-0.1cm S1 heat 400C | 27.0 | 18.0 | 16.0 | 18.0 | 20.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 6419.0000 | 6401.8884 | 6419.0000 |
| 2.0164 | 6159.7296 | 6380.0042 | 6377.2419 |
| 2.0274 | 6141.5152 | 6338.3341 | 6335.4837 |
| 2.0384 | 6273.2566 | 6296.6683 | 6293.7256 |
| 2.0494 | 6069.2793 | 6255.0070 | 6251.9675 |
| 2.0604 | 6027.7035 | 6213.3505 | 6210.2093 |
| 2.0714 | 5906.7522 | 6171.6992 | 6168.4512 |
| 2.0824 | 5980.1185 | 6130.0534 | 6126.6931 |
| 2.0934 | 5981.3805 | 6088.4135 | 6084.9349 |
| 2.1044 | 5892.6283 | 6046.7800 | 6043.1768 |
| 2.1154 | 5970.4808 | 6005.1531 | 6001.4187 |
| 2.1264 | 6003.6893 | 5963.5336 | 5959.6605 |
| 2.1374 | 5826.1976 | 5921.9218 | 5917.9024 |
| 2.1484 | 5834.9263 | 5880.3184 | 5876.1443 |
| 2.1594 | 5936.7473 | 5838.7240 | 5834.3861 |
| 2.1704 | 5816.0959 | 5797.1394 | 5792.6280 |
| 2.1814 | 5843.0531 | 5755.5654 | 5750.8698 |
| 2.1924 | 5599.1937 | 5716.5390 | 5709.1117 |
| 2.2034 | 5640.6372 | 5677.8041 | 5672.7053 |
| 2.2144 | 5680.8142 | 5641.6188 | 5636.2989 |
| 2.2254 | 5691.5064 | 5605.4482 | 5599.8924 |
| 2.2364 | 5557.8392 | 5569.2933 | 5563.4860 |
| 2.2474 | 5546.5310 | 5533.1558 | 5527.0796 |
| 2.2584 | 5510.9617 | 5497.0371 | 5490.6732 |
| 2.2694 | 5513.5870 | 5460.9391 | 5454.2667 |
| 2.2804 | 5401.9435 | 5424.8638 | 5417.8603 |
| 2.2914 | 5380.7827 | 5388.8134 | 5381.4539 |
| 2.3024 | 5415.3009 | 5352.7904 | 5345.0475 |
| 2.3134 | 5343.6185 | 5316.7977 | 5308.6410 |
| 2.3244 | 5174.7227 | 5280.8386 | 5272.2346 |
| 2.3354 | 5136.3953 | 5244.9167 | 5235.8282 |
| 2.3464 | 5159.4425 | 5209.0363 | 5199.4217 |
| 2.3574 | 5282.7866 | 5173.2024 | 5163.0153 |
| 2.3684 | 5172.8643 | 5137.4207 | 5126.6089 |
| 2.3794 | 4992.0305 | 5101.6550 | 5090.2025 |
| 2.3904 | 5039.2714 | 5065.9523 | 5053.7047 |
| 2.4014 | 5098.7168 | 5030.2846 | 5017.2070 |
| 2.4124 | 5064.8240 | 4994.7090 | 4980.7093 |
| 2.4234 | 5028.0905 | 4959.2433 | 4944.2115 |
| 2.4344 | 4968.5619 | 4923.9112 | 4907.7138 |
| 2.4454 | 5004.3648 | 4888.7450 | 4871.2161 |
| 2.4564 | 5021.8348 | 4853.7884 | 4834.7183 |
| 2.4674 | 4957.1209 | 4819.1004 | 4798.2206 |
| 2.4784 | 4945.5969 | 4784.7602 | 4761.7229 |
| 2.4894 | 4911.9705 | 4750.8726 | 4725.2251 |
| 2.5004 | 4854.3628 | 4717.5729 | 4688.7274 |
| 2.5114 | 4768.1494 | 4685.0319 | 4652.2297 |
| 2.5224 | 4760.8796 | 4653.4586 | 4615.7319 |
| 2.5334 | 4774.4513 | 4623.1002 | 4579.2342 |
| 2.5444 | 4719.8643 | 4594.2374 | 4542.7365 |
| 2.5554 | 4699.0728 | 4567.1740 | 4506.2387 |
| 2.5664 | 4660.2552 | 4542.2202 | 4469.7410 |
| 2.5774 | 4618.1042 | 4519.6680 | 4433.2433 |
| 2.5884 | 4575.4287 | 4499.7617 | 4396.7455 |
| 2.5994 | 4567.2920 | 4482.6613 | 4360.2478 |
| 2.6104 | 4588.2242 | 4468.4037 | 4323.7501 |
| 2.6214 | 4551.9489 | 4456.8583 | 4287.2523 |
| 2.6324 | 4470.3481 | 4447.6795 | 4250.7546 |
| 2.6434 | 4452.5546 | 4440.2494 | 4214.2569 |
| 2.6544 | 4436.4204 | 4433.6125 | 4177.7591 |
| 2.6654 | 4360.4159 | 4426.4108 | 4141.2614 |
| 2.6764 | 4431.9685 | 4416.8545 | 4104.7637 |
| 2.6874 | 4407.6086 | 4402.8019 | 4068.2659 |
| 2.6984 | 4265.3318 | 4382.0303 | 4031.7682 |
| 2.7094 | 4210.1209 | 4352.7083 | 3995.2705 |
| 2.7204 | 4139.4887 | 4313.9202 | 3958.7727 |
| 2.7314 | 4161.9381 | 4265.9693 | 3922.2750 |
| 2.7424 | 4151.2360 | 4210.2716 | 3885.7773 |
| 2.7534 | 4098.5241 | 4148.8671 | 3849.2795 |
| 2.7644 | 4093.2404 | 4084.0202 | 3812.6905 |
| 2.7754 | 4012.2645 | 4017.6814 | 3776.1014 |
| 2.7864 | 4003.3633 | 3951.4766 | 3739.5124 |
| 2.7974 | 3763.2920 | 3886.5646 | 3702.9234 |
| 2.8084 | 3838.7724 | 3823.7315 | 3666.3343 |
| 2.8194 | 3730.9410 | 3763.4582 | 3629.7453 |
| 2.8304 | 3700.5634 | 3705.9818 | 3593.1562 |
| 2.8414 | 3521.5172 | 3651.3475 | 3556.5672 |
| 2.8524 | 3618.7837 | 3599.4547 | 3519.9781 |
| 2.8634 | 3453.3923 | 3550.0988 | 3483.3891 |
| 2.8744 | 3518.8245 | 3503.0087 | 3446.8001 |
| 2.8854 | 3497.4012 | 3457.8804 | 3410.2110 |
| 2.8964 | 3424.3230 | 3414.4045 | 3373.6220 |
| 2.9074 | 3349.9528 | 3372.2866 | 3337.0329 |
| 2.9184 | 3344.2419 | 3331.2613 | 3300.4439 |
| 2.9294 | 3351.5546 | 3291.0993 | 3263.8549 |
| 2.9404 | 3214.5260 | 3256.7148 | 3227.2658 |
| 2.9514 | 3121.2242 | 3223.4116 | 3201.4479 |
| 2.9624 | 3148.2256 | 3195.6124 | 3175.6300 |
| 2.9734 | 3021.1623 | 3168.1207 | 3149.8121 |
| 2.9844 | 3070.5354 | 3140.8673 | 3123.9942 |
| 2.9954 | 3093.4071 | 3113.8012 | 3098.1763 |
| 3.0064 | 3075.2606 | 3086.8845 | 3072.3584 |
| 3.0174 | 3025.3530 | 3060.0893 | 3046.5405 |
| 3.0284 | 2939.3024 | 3033.3949 | 3020.7226 |
| 3.0394 | 3021.7591 | 3006.7856 | 2994.9047 |
| 3.0504 | 3070.3141 | 2980.2493 | 2969.0868 |
| 3.0614 | 2908.8614 | 2953.7765 | 2943.2689 |
| 3.0724 | 2894.6136 | 2927.3595 | 2917.4510 |
| 3.0834 | 2907.8643 | 2900.9918 | 2891.6330 |
| 3.0944 | 2886.6018 | 2874.6682 | 2865.8151 |
| 3.1054 | 2887.5231 | 2848.3840 | 2839.9972 |
| 3.1164 | 2835.1018 | 2822.1352 | 2814.1793 |
| 3.1274 | 2773.4454 | 2799.9142 | 2788.3614 |
| 3.1384 | 2766.9857 | 2778.1619 | 2770.9751 |
| 3.1494 | 2668.9400 | 2760.4317 | 2753.5887 |
| 3.1604 | 2712.6194 | 2742.7253 | 2736.2024 |
| 3.1714 | 2647.5084 | 2725.0406 | 2718.8160 |
| 3.1824 | 2685.6603 | 2707.3757 | 2701.4297 |
| 3.1934 | 2695.6106 | 2689.7289 | 2684.0433 |
| 3.2044 | 2659.2439 | 2672.0986 | 2666.6570 |
| 3.2154 | 2663.7286 | 2654.4836 | 2649.2707 |
| 3.2264 | 2668.5988 | 2636.8826 | 2631.8843 |
| 3.2374 | 2597.2232 | 2619.2944 | 2614.4980 |
| 3.2484 | 2556.6667 | 2601.7182 | 2597.1116 |
| 3.2594 | 2596.4307 | 2584.1529 | 2579.7253 |
| 3.2704 | 2573.5472 | 2566.5977 | 2562.3389 |
| 3.2814 | 2524.9607 | 2549.0520 | 2544.9526 |
| 3.2924 | 2517.2301 | 2531.5150 | 2527.5662 |
| 3.3034 | 2492.4966 | 2513.9860 | 2510.1799 |
| 3.3144 | 2512.9076 | 2498.0494 | 2492.7935 |
| 3.3254 | 2493.6076 | 2482.2943 | 2478.7512 |
| 3.3364 | 2421.4602 | 2468.1305 | 2464.7089 |
| 3.3474 | 2443.4602 | 2453.9728 | 2450.6666 |
| 3.3584 | 2433.8436 | 2439.8209 | 2436.6243 |
| 3.3694 | 2375.5182 | 2425.6742 | 2422.5820 |
| 3.3804 | 2365.4636 | 2411.5326 | 2408.5397 |
| 3.3914 | 2387.4956 | 2397.3957 | 2394.4974 |
| 3.4024 | 2380.1957 | 2383.2631 | 2380.4552 |
| 3.4134 | 2356.5605 | 2369.1347 | 2366.4129 |
| 3.4244 | 2336.4336 | 2355.0101 | 2352.3706 |
| 3.4354 | 2302.4779 | 2340.8893 | 2338.3283 |
| 3.4464 | 2295.9317 | 2326.7718 | 2324.2860 |
| 3.4574 | 2291.6637 | 2312.6576 | 2310.2437 |
| 3.4684 | 2277.1141 | 2298.5465 | 2296.2014 |
| 3.4794 | 2284.9400 | 2284.4382 | 2282.1591 |
| 3.4904 | 2299.2522 | 2270.3327 | 2268.1168 |
| 3.5014 | 2229.7974 | 2256.2298 | 2254.0745 |
| 3.5124 | 2252.8132 | 2242.1293 | 2240.0322 |
| 3.5234 | 2234.7492 | 2228.0312 | 2225.9899 |
| 3.5344 | 2202.2478 | 2213.9352 | 2211.9476 |
| 3.5454 | 2170.3323 | 2199.8413 | 2197.9053 |
| 3.5564 | 2173.1947 | 2185.7494 | 2183.8630 |
| 3.5674 | 2192.1613 | 2171.6594 | 2169.8207 |
| 3.5784 | 2154.5732 | 2157.5711 | 2155.7784 |
| 3.5894 | 2154.8584 | 2143.5392 | 2141.7361 |
| 3.6004 | 2156.6534 | 2129.4933 | 2127.6938 |
| 3.6114 | 2071.7836 | 2115.4387 | 2113.6515 |
| 3.6224 | 2075.0103 | 2101.3777 | 2099.6092 |
| 3.6334 | 2045.7797 | 2087.2990 | 2085.5669 |
| 3.6444 | 2067.9292 | 2073.2217 | 2071.5246 |
| 3.6554 | 2043.6283 | 2059.1457 | 2057.4823 |
| 3.6664 | 2022.5929 | 2045.0710 | 2043.4400 |
| 3.6774 | 1984.4022 | 2030.9974 | 2029.3977 |
| 3.6884 | 2013.3407 | 2019.5052 | 2015.3554 |
| 3.6994 | 2042.1062 | 2005.8071 | 2004.2666 |
| 3.7104 | 2023.2773 | 1994.6903 | 1993.1777 |
| 3.7214 | 2009.0737 | 1983.5745 | 1982.0888 |
| 3.7324 | 1993.1249 | 1972.4596 | 1971.0000 |
| 3.7434 | 1982.5801 | 1961.3457 | 1959.9111 |
| 3.7544 | 1972.4572 | 1950.2327 | 1948.8222 |
| 3.7654 | 1948.8024 | 1939.1206 | 1937.7334 |
| 3.7764 | 1889.2684 | 1928.0093 | 1926.6445 |
| 3.7874 | 1916.7434 | 1916.8988 | 1915.5556 |
| 3.7984 | 1914.0585 | 1905.7891 | 1904.4668 |
| 3.8094 | 1930.5437 | 1894.6801 | 1893.3779 |
| 3.8204 | 1901.6917 | 1883.5718 | 1882.2890 |
| 3.8314 | 1890.8791 | 1872.4643 | 1871.2002 |
| 3.8424 | 1887.2635 | 1861.3574 | 1860.1113 |
| 3.8534 | 1869.4572 | 1850.2512 | 1849.0224 |
| 3.8644 | 1804.3859 | 1839.1456 | 1837.9336 |
| 3.8754 | 1816.4268 | 1829.0465 | 1826.8447 |
| 3.8864 | 1878.6681 | 1818.0876 | 1816.9072 |
| 3.8974 | 1767.8437 | 1808.1351 | 1806.9696 |
| 3.9084 | 1826.5595 | 1798.1833 | 1797.0321 |
| 3.9194 | 1858.0678 | 1788.2319 | 1787.0946 |
| 3.9304 | 1809.7173 | 1778.2811 | 1777.1571 |
| 3.9414 | 1778.2045 | 1768.3308 | 1767.2196 |
| 3.9524 | 1763.7345 | 1758.3810 | 1757.2820 |
| 3.9634 | 1749.1416 | 1748.4317 | 1747.3445 |
| 3.9744 | 1803.2050 | 1738.4829 | 1737.4070 |
| 3.9854 | 1821.4867 | 1728.5346 | 1727.4695 |
| 3.9964 | 1737.7753 | 1718.5867 | 1717.5320 |
| 4.0074 | 1727.7581 | 1708.6393 | 1707.5944 |
| 4.0184 | 1705.7271 | 1698.6923 | 1697.6569 |
| 4.0294 | 1717.2301 | 1688.7458 | 1687.7194 |
| 4.0404 | 1677.4277 | 1678.7997 | 1677.7819 |
| 4.0514 | 1656.8525 | 1668.8540 | 1667.8443 |
| 4.0624 | 1647.8063 | 1660.8093 | 1657.9068 |
| 4.0734 | 1661.7788 | 1651.1393 | 1650.1448 |
| 4.0844 | 1675.4203 | 1643.3704 | 1642.3828 |
| 4.0954 | 1633.0413 | 1635.6018 | 1634.6208 |
| 4.1064 | 1662.9892 | 1627.8336 | 1626.8587 |
| 4.1174 | 1680.0442 | 1620.0658 | 1619.0967 |
| 4.1284 | 1631.6922 | 1612.2984 | 1611.3347 |
| 4.1394 | 1588.6155 | 1604.5314 | 1603.5727 |
| 4.1504 | 1632.8334 | 1596.7648 | 1595.8106 |
| 4.1614 | 1672.7758 | 1588.9986 | 1588.0486 |
| 4.1724 | 1608.4051 | 1581.2327 | 1580.2866 |
| 4.1834 | 1578.1681 | 1573.4672 | 1572.5246 |
| 4.1944 | 1590.3643 | 1565.7021 | 1564.7625 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 8 Etosha22 Crt 0-0.1cm S1 heat 400C | 2.0054 | 29.9894 | 0.0110 | 12/4/2023 12:01:57 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.7101 | 320.45 | 0.1732 | 32.57406 | 31.52 |
| 5.3254 | 98.92 | 0.1732 | 16.58135 | 9.73 |
| 7.1276 | 1016.70 | 0.1732 | 12.39217 | 100.00 |
| 8.6847 | 329.56 | 0.2598 | 10.17360 | 32.41 |
| 15.7594 | 300.99 | 0.1515 | 5.61876 | 29.61 |
| 18.2159 | 31.10 | 0.2165 | 4.86622 | 3.06 |
| 19.6643 | 29.17 | 0.3464 | 4.51095 | 2.87 |
| 25.9209 | 184.02 | 0.1299 | 3.43457 | 18.10 |
| 26.6960 | 68.73 | 0.1299 | 3.33658 | 6.76 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-011-6753 | 51 | Sodium Aluminum Silicate Hydrate | Na8 Al8 Si16 O48 ( H2 O )8 | Analcime | 27 |
| * | 04-017-4317 | 25 | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | K Mg0.2 Mn0.1 Fe2.4 Al1.7 Si2.6 O10 ( O H )2 | Biotite-1M | 18 |
| * | 04-017-7286 | 27 | Potassium Manganese Aluminum Silicon Oxide Hydroxide Hydrate | K0.8 Mn4 Al1.08 Si4.92 O16 ( O H )2 ( H2 O )3 | Ganophyllite | 16 |
| * | 04-025-4215 | 6 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 18 |
| * | 01-080-5017 | 17 | Magnesium Silicate Hydroxide Hydrate | Mg7.73 ( Si12 O30 ) ( O H )4 ( H2 O )4 ( H2 O )6 | Sepiolite | 20 |

Anchor Scan Parameters

Dataset Name	8 Etosha22 Crt 0-0.1cm S1 heat 400C

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 8\8 Etosha22 Crt 0-0.1cm S1 heat 400C.xrdml

Sample Identification	8 Etosha22 Crt 0-0.1cm S1 heat 400C

Measurement Start Date/Time	12/4/2023 12:01:57 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes