8 Etosha 22 CRT 0-0.1 cm S1 550 C

Graphics

Graphics

Graphics

Quantitative Results

Phase Potassium Sodium Magnesium Manganese Aluminum Iron Silicon Titanium Oxide Hydroxide

Weight fraction/ %	32.0

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	24.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	44.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Potassium Sodium Magnesium Manganese Aluminum Iron Silicon Titanium Oxide Hydroxide | Sodium Aluminum Silicate Hydrate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide |
| --- | --- | --- | --- |
| 8 Etosha22 Crt 0-0.1cm S1 heat 550C | 32.0 | 24.0 | 44.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 7702.0000 | 7703.0253 | 7702.0000 |
| 2.0164 | 7511.3889 | 7674.0886 | 7649.9883 |
| 2.0274 | 7618.9440 | 7622.8636 | 7597.9767 |
| 2.0384 | 7451.4366 | 7571.6772 | 7545.9650 |
| 2.0494 | 7291.0619 | 7520.5321 | 7493.9533 |
| 2.0604 | 7501.4970 | 7469.4312 | 7441.9417 |
| 2.0714 | 7432.0708 | 7418.3776 | 7389.9300 |
| 2.0824 | 7227.5261 | 7367.3749 | 7337.9184 |
| 2.0934 | 7168.2989 | 7316.4271 | 7285.9067 |
| 2.1044 | 7077.1504 | 7265.5386 | 7233.8950 |
| 2.1154 | 7212.8997 | 7214.7147 | 7181.8834 |
| 2.1264 | 7252.5664 | 7163.9610 | 7129.8717 |
| 2.1374 | 7201.0118 | 7113.2845 | 7077.8600 |
| 2.1484 | 7005.3033 | 7062.6930 | 7025.8484 |
| 2.1594 | 7057.7827 | 7012.1958 | 6973.8367 |
| 2.1704 | 7006.3746 | 6961.8038 | 6921.8250 |
| 2.1814 | 7001.8319 | 6911.5298 | 6869.8134 |
| 2.1924 | 6861.2832 | 6861.2893 | 6817.8017 |
| 2.2034 | 6834.7522 | 6811.2349 | 6765.6241 |
| 2.2144 | 6645.1790 | 6761.2540 | 6713.4465 |
| 2.2254 | 6813.9046 | 6711.4728 | 6661.2689 |
| 2.2364 | 6790.9041 | 6661.9221 | 6609.0913 |
| 2.2474 | 6749.2969 | 6612.6384 | 6556.9136 |
| 2.2584 | 6579.7768 | 6563.6649 | 6504.7360 |
| 2.2694 | 6595.3068 | 6515.0521 | 6452.5584 |
| 2.2804 | 6749.6146 | 6466.8586 | 6400.3808 |
| 2.2914 | 6713.6106 | 6419.1524 | 6348.2032 |
| 2.3024 | 6600.8142 | 6372.0113 | 6296.0255 |
| 2.3134 | 6503.3707 | 6325.5235 | 6243.8479 |
| 2.3244 | 6457.1190 | 6279.7883 | 6191.6703 |
| 2.3354 | 6449.5015 | 6234.9159 | 6139.4927 |
| 2.3464 | 6333.0831 | 6191.0273 | 6087.3151 |
| 2.3574 | 6244.0924 | 6148.2540 | 6035.1375 |
| 2.3684 | 6289.4410 | 6106.7359 | 5982.9598 |
| 2.3794 | 6304.9705 | 6066.5395 | 5930.7822 |
| 2.3904 | 6256.5850 | 6027.9260 | 5878.4703 |
| 2.4014 | 6275.6018 | 5990.9407 | 5826.1585 |
| 2.4124 | 6268.7748 | 5955.8170 | 5773.8466 |
| 2.4234 | 6150.8564 | 5922.7009 | 5721.5347 |
| 2.4344 | 6040.1711 | 5891.7279 | 5669.2228 |
| 2.4454 | 5995.9636 | 5863.0167 | 5616.9110 |
| 2.4564 | 6057.4882 | 5836.6639 | 5564.5991 |
| 2.4674 | 6026.0590 | 5812.7376 | 5512.2872 |
| 2.4784 | 6028.1254 | 5791.2708 | 5459.9753 |
| 2.4894 | 5943.0531 | 5772.2549 | 5407.6634 |
| 2.5004 | 5961.3850 | 5755.6321 | 5355.3516 |
| 2.5114 | 5856.8102 | 5741.2881 | 5303.0397 |
| 2.5224 | 5738.3501 | 5729.0440 | 5250.7278 |
| 2.5334 | 5783.8289 | 5718.6468 | 5198.4159 |
| 2.5444 | 5757.4439 | 5709.7596 | 5146.1041 |
| 2.5554 | 5721.3963 | 5701.9502 | 5093.7922 |
| 2.5664 | 5798.1165 | 5694.6797 | 5041.4803 |
| 2.5774 | 5730.0383 | 5687.2913 | 4989.1684 |
| 2.5884 | 5667.2571 | 5679.0032 | 4936.8565 |
| 2.5994 | 5611.9203 | 5668.9073 | 4884.5447 |
| 2.6104 | 5614.0964 | 5655.9816 | 4832.2328 |
| 2.6214 | 5583.5723 | 5639.1201 | 4779.9209 |
| 2.6324 | 5398.3613 | 5617.1843 | 4727.6090 |
| 2.6434 | 5390.0207 | 5589.0793 | 4675.2972 |
| 2.6544 | 5367.8638 | 5553.8457 | 4622.9853 |
| 2.6654 | 5340.4130 | 5510.7572 | 4570.6734 |
| 2.6764 | 5319.7557 | 5459.4032 | 4518.3615 |
| 2.6874 | 5186.7384 | 5399.7400 | 4466.0496 |
| 2.6984 | 5172.5531 | 5332.0963 | 4413.7378 |
| 2.7094 | 5054.9262 | 5257.1322 | 4361.4259 |
| 2.7204 | 5029.7881 | 5175.7619 | 4309.1140 |
| 2.7314 | 4953.3127 | 5089.0583 | 4256.8021 |
| 2.7424 | 4862.5319 | 4998.1578 | 4204.4903 |
| 2.7534 | 4613.8141 | 4904.0989 | 4152.1784 |
| 2.7644 | 4529.8363 | 4808.0354 | 4099.7322 |
| 2.7754 | 4550.5320 | 4710.7946 | 4047.2861 |
| 2.7864 | 4288.8372 | 4613.2687 | 3994.8400 |
| 2.7974 | 4269.4690 | 4516.1428 | 3942.3938 |
| 2.8084 | 4225.3432 | 4419.9818 | 3889.9477 |
| 2.8194 | 4082.6598 | 4325.2412 | 3837.5016 |
| 2.8304 | 4040.4233 | 4232.2786 | 3785.0554 |
| 2.8414 | 3962.3363 | 4141.3652 | 3732.6093 |
| 2.8524 | 3849.1091 | 4052.6961 | 3680.1631 |
| 2.8634 | 3821.9086 | 3966.3994 | 3627.7170 |
| 2.8744 | 3702.5388 | 3882.5452 | 3575.2709 |
| 2.8854 | 3636.0698 | 3801.1526 | 3522.8247 |
| 2.8964 | 3541.4159 | 3722.1976 | 3470.3786 |
| 2.9074 | 3564.6391 | 3645.6194 | 3417.9325 |
| 2.9184 | 3392.7178 | 3571.3273 | 3365.4863 |
| 2.9294 | 3373.5486 | 3499.2072 | 3313.0402 |
| 2.9404 | 3211.9843 | 3442.1960 | 3260.5940 |
| 2.9514 | 3225.4720 | 3382.5971 | 3229.8025 |
| 2.9624 | 3109.9425 | 3337.8115 | 3199.0109 |
| 2.9734 | 3219.1455 | 3294.6163 | 3168.2194 |
| 2.9844 | 3098.0329 | 3252.8583 | 3137.4278 |
| 2.9954 | 3106.8319 | 3212.3888 | 3106.6362 |
| 3.0064 | 3090.0093 | 3173.0657 | 3075.8447 |
| 3.0174 | 3025.9685 | 3134.7556 | 3045.0531 |
| 3.0284 | 2933.1239 | 3097.3351 | 3014.2616 |
| 3.0394 | 2879.6146 | 3060.6913 | 2983.4700 |
| 3.0504 | 3009.5089 | 3024.7226 | 2952.6784 |
| 3.0614 | 2999.1858 | 2989.3381 | 2921.8869 |
| 3.0724 | 2905.6971 | 2954.4577 | 2891.0953 |
| 3.0834 | 2835.3884 | 2920.0113 | 2860.3038 |
| 3.0944 | 2773.4071 | 2885.9382 | 2829.5122 |
| 3.1054 | 2796.5664 | 2852.1861 | 2798.7206 |
| 3.1164 | 2756.9317 | 2818.7103 | 2767.9291 |
| 3.1274 | 2760.8997 | 2792.8750 | 2737.1375 |
| 3.1384 | 2694.2557 | 2764.7065 | 2718.6110 |
| 3.1494 | 2697.0954 | 2744.1194 | 2700.0845 |
| 3.1604 | 2704.7994 | 2723.6888 | 2681.5580 |
| 3.1714 | 2738.8122 | 2703.3956 | 2663.0315 |
| 3.1824 | 2641.7940 | 2683.2238 | 2644.5050 |
| 3.1934 | 2599.6725 | 2663.1600 | 2625.9785 |
| 3.2044 | 2553.5752 | 2643.1927 | 2607.4520 |
| 3.2154 | 2574.2782 | 2623.3124 | 2588.9255 |
| 3.2264 | 2536.5162 | 2603.5109 | 2570.3990 |
| 3.2374 | 2587.0914 | 2583.7812 | 2551.8725 |
| 3.2484 | 2542.5000 | 2564.1173 | 2533.3460 |
| 3.2594 | 2479.3599 | 2544.5138 | 2514.8195 |
| 3.2704 | 2446.1824 | 2524.9662 | 2496.2930 |
| 3.2814 | 2442.9017 | 2505.4703 | 2477.7665 |
| 3.2924 | 2482.7124 | 2486.0226 | 2459.2400 |
| 3.3034 | 2463.4159 | 2466.6197 | 2440.7135 |
| 3.3144 | 2387.7188 | 2449.6429 | 2422.1870 |
| 3.3254 | 2391.0207 | 2431.8874 | 2407.6109 |
| 3.3364 | 2407.8707 | 2416.5528 | 2393.0349 |
| 3.3474 | 2474.4199 | 2401.2528 | 2378.4588 |
| 3.3584 | 2416.7905 | 2385.9853 | 2363.8827 |
| 3.3694 | 2296.5782 | 2370.7483 | 2349.3067 |
| 3.3804 | 2335.8919 | 2355.5401 | 2334.7306 |
| 3.3914 | 2333.1150 | 2340.3591 | 2320.1545 |
| 3.4024 | 2342.9749 | 2325.2038 | 2305.5785 |
| 3.4134 | 2287.1711 | 2310.0726 | 2291.0024 |
| 3.4244 | 2166.1032 | 2294.9644 | 2276.4263 |
| 3.4354 | 2211.4799 | 2279.8779 | 2261.8503 |
| 3.4464 | 2231.9518 | 2264.8119 | 2247.2742 |
| 3.4574 | 2285.4248 | 2249.7654 | 2232.6981 |
| 3.4684 | 2273.9720 | 2234.7373 | 2218.1221 |
| 3.4794 | 2193.4159 | 2219.7267 | 2203.5460 |
| 3.4904 | 2198.3274 | 2204.7328 | 2188.9699 |
| 3.5014 | 2136.0963 | 2190.9635 | 2174.3939 |
| 3.5124 | 2172.5423 | 2176.7945 | 2161.8207 |
| 3.5234 | 2188.2035 | 2163.8486 | 2149.2475 |
| 3.5344 | 2164.4140 | 2150.9163 | 2136.6744 |
| 3.5454 | 2078.7178 | 2137.9970 | 2124.1012 |
| 3.5564 | 2093.4484 | 2125.0900 | 2111.5280 |
| 3.5674 | 2110.0000 | 2112.1948 | 2098.9548 |
| 3.5784 | 2085.7561 | 2099.3492 | 2086.3817 |
| 3.5894 | 2072.6106 | 2086.5501 | 2073.8085 |
| 3.6004 | 2092.1195 | 2073.7079 | 2061.2353 |
| 3.6114 | 2017.7561 | 2060.8936 | 2048.6621 |
| 3.6224 | 2025.2375 | 2048.0519 | 2036.0890 |
| 3.6334 | 2031.1809 | 2035.2192 | 2023.5158 |
| 3.6444 | 2029.3373 | 2022.3951 | 2010.9426 |
| 3.6554 | 2029.8437 | 2009.5793 | 1998.3694 |
| 3.6664 | 2029.1441 | 1996.7713 | 1985.7963 |
| 3.6774 | 1993.4022 | 1983.9710 | 1973.2231 |
| 3.6884 | 1956.3009 | 1971.2991 | 1960.6499 |
| 3.6994 | 1921.6440 | 1958.5615 | 1948.2466 |
| 3.7104 | 1920.7153 | 1945.9519 | 1935.8434 |
| 3.7214 | 1879.7168 | 1933.3487 | 1923.4401 |
| 3.7324 | 1864.8437 | 1920.7517 | 1911.0368 |
| 3.7434 | 1939.3589 | 1908.1606 | 1898.6335 |
| 3.7544 | 1946.8628 | 1895.5752 | 1886.2302 |
| 3.7654 | 1963.4317 | 1882.9952 | 1873.8270 |
| 3.7764 | 1817.1710 | 1870.4205 | 1861.4237 |
| 3.7874 | 1803.0973 | 1857.8509 | 1849.0204 |
| 3.7984 | 1848.2994 | 1845.2862 | 1836.6171 |
| 3.8094 | 1932.6086 | 1832.7262 | 1824.2138 |
| 3.8204 | 1786.6431 | 1820.1707 | 1811.8106 |
| 3.8314 | 1906.9528 | 1807.6196 | 1799.4073 |
| 3.8424 | 1766.4194 | 1795.0728 | 1787.0040 |
| 3.8534 | 1823.6519 | 1782.5300 | 1774.6007 |
| 3.8644 | 1756.6775 | 1769.9911 | 1762.1974 |
| 3.8754 | 1712.8742 | 1759.8533 | 1749.7942 |
| 3.8864 | 1786.0796 | 1748.2839 | 1740.7502 |
| 3.8974 | 1728.0797 | 1739.1154 | 1731.7062 |
| 3.9084 | 1753.3899 | 1729.9502 | 1722.6622 |
| 3.9194 | 1773.3983 | 1720.7884 | 1713.6182 |
| 3.9304 | 1824.5668 | 1711.6298 | 1704.5742 |
| 3.9414 | 1738.5536 | 1702.4744 | 1695.5302 |
| 3.9524 | 1696.2331 | 1693.3219 | 1686.4862 |
| 3.9634 | 1733.7876 | 1684.1723 | 1677.4422 |
| 3.9744 | 1682.0069 | 1675.0256 | 1668.3982 |
| 3.9854 | 1728.2301 | 1665.8816 | 1659.3542 |
| 3.9964 | 1690.8766 | 1656.7403 | 1650.3102 |
| 4.0074 | 1680.8387 | 1647.6016 | 1641.2662 |
| 4.0184 | 1654.5192 | 1638.4654 | 1632.2223 |
| 4.0294 | 1627.6765 | 1629.3316 | 1623.1783 |
| 4.0404 | 1623.1569 | 1620.2002 | 1614.1343 |
| 4.0514 | 1650.5487 | 1611.0711 | 1605.0903 |
| 4.0624 | 1619.1623 | 1601.9442 | 1596.0463 |
| 4.0734 | 1624.1927 | 1592.8196 | 1587.0023 |
| 4.0844 | 1577.9734 | 1583.6970 | 1577.9583 |
| 4.0954 | 1568.1888 | 1574.5765 | 1568.9143 |
| 4.1064 | 1618.4439 | 1565.4581 | 1559.8703 |
| 4.1174 | 1569.6076 | 1556.3416 | 1550.8263 |
| 4.1284 | 1550.7026 | 1547.2270 | 1541.7823 |
| 4.1394 | 1602.4563 | 1538.1143 | 1532.7383 |
| 4.1504 | 1577.1828 | 1529.0035 | 1523.6943 |
| 4.1614 | 1495.3648 | 1519.8944 | 1514.6503 |
| 4.1724 | 1503.1736 | 1510.7871 | 1505.6064 |
| 4.1834 | 1545.4071 | 1501.6816 | 1496.5624 |
| 4.1944 | 1515.2999 | 1492.5777 | 1487.5184 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 8 Etosha22 Crt 0-0.1cm S1 heat 550C | 2.0054 | 29.9894 | 0.0110 | 12/4/2023 3:12:36 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.6700 | 840.92 | 0.3031 | 33.06311 | 100.00 |
| 5.3171 | 119.17 | 0.1732 | 16.60722 | 14.17 |
| 8.6950 | 392.12 | 0.2598 | 10.16154 | 46.63 |
| 10.6626 | 28.42 | 0.4330 | 8.29039 | 3.38 |
| 15.9104 | 171.70 | 0.1082 | 5.56580 | 20.42 |
| 17.4786 | 14.76 | 0.5196 | 5.06980 | 1.76 |
| 19.7802 | 14.95 | 0.6927 | 4.48476 | 1.78 |
| 26.2520 | 126.51 | 0.1515 | 3.39200 | 15.04 |
| 27.5499 | 43.12 | 0.4330 | 3.23507 | 5.13 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-015-8236 | 37 | Potassium Sodium Magnesium Manganese Aluminum Iron Silicon Titanium Oxide Hydroxide | K0.94 Na0.01 Mg0.71 Ti0.13 Mn0.07 Fe1.49 Al1.59 Si2.79 O10.14 ( O H )1.86 | Biotite-1M | 32 |
| * | 01-076-6569 | 30 | Sodium Aluminum Silicate Hydrate | Na0.9 ( ( Al0.9 Si2 ) O6 ) ( H2 O ) | Analcime | 24 |
| * | 04-025-4215 | 17 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 44 |

Anchor Scan Parameters

Dataset Name	8 Etosha22 Crt 0-0.1cm S1 heat 550C

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 8\8 Etosha22 Crt 0-0.1cm S1 heat 550C.xrdml

Sample Identification	8 Etosha22 Crt 0-0.1cm S1 heat 550C

Measurement Start Date/Time	12/4/2023 3:12:36 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes