8 Etosha 22 CRT 0-0.1 cm S1 GLYCOLATED

Graphics

Graphics

Graphics

Quantitative Results

Phase Potassium Calcium Manganese Aluminum Silicate Hydroxide Hydrate

Weight fraction/ %	20.0

Phase Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide

Weight fraction/ %	17.0

Phase Magnesium Silicate Hydroxide Hydrate

Weight fraction/ %	10.0

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	22.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	31.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Potassium Calcium Manganese Aluminum Silicate Hydroxide Hydrate | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | Magnesium Silicate Hydroxide Hydrate | Sodium Aluminum Silicate Hydrate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide |
| --- | --- | --- | --- | --- | --- |
| 8 Etosha22 crt 0-0.1cm S1 glycolated | 20.0 | 17.0 | 10.0 | 22.0 | 31.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 5920.0000 | 5904.2628 | 5920.0000 |
| 2.0164 | 5833.4671 | 5892.4044 | 5886.6518 |
| 2.0274 | 5870.8525 | 5859.2597 | 5853.3035 |
| 2.0384 | 5863.0088 | 5826.1259 | 5819.9553 |
| 2.0494 | 5801.7571 | 5793.0038 | 5786.6071 |
| 2.0604 | 5617.6534 | 5759.8942 | 5753.2589 |
| 2.0714 | 5542.8584 | 5726.7980 | 5719.9106 |
| 2.0824 | 5632.1834 | 5693.7162 | 5686.5624 |
| 2.0934 | 5651.3491 | 5660.6501 | 5653.2142 |
| 2.1044 | 5535.2522 | 5627.6007 | 5619.8659 |
| 2.1154 | 5669.0944 | 5594.5694 | 5586.5177 |
| 2.1264 | 5566.0487 | 5561.5577 | 5553.1695 |
| 2.1374 | 5508.5369 | 5528.5672 | 5519.8212 |
| 2.1484 | 5565.3412 | 5495.5998 | 5486.4730 |
| 2.1594 | 5483.0000 | 5462.6574 | 5453.1248 |
| 2.1704 | 5468.4351 | 5429.7423 | 5419.7766 |
| 2.1814 | 5382.9577 | 5396.8569 | 5386.4283 |
| 2.1924 | 5323.5364 | 5364.5123 | 5353.0801 |
| 2.2034 | 5370.9026 | 5331.9830 | 5320.5275 |
| 2.2144 | 5212.9577 | 5300.0013 | 5287.9749 |
| 2.2254 | 5300.3795 | 5268.0637 | 5255.4222 |
| 2.2364 | 5255.8348 | 5236.1753 | 5222.8696 |
| 2.2474 | 5198.7856 | 5204.3423 | 5190.3170 |
| 2.2584 | 5218.0462 | 5172.5725 | 5157.7644 |
| 2.2694 | 5197.9321 | 5140.8752 | 5125.2117 |
| 2.2804 | 5123.8840 | 5109.2625 | 5092.6591 |
| 2.2914 | 5165.3520 | 5077.7494 | 5060.1065 |
| 2.3024 | 5124.2920 | 5046.3554 | 5027.5539 |
| 2.3134 | 5104.7994 | 5015.1049 | 4995.0012 |
| 2.3244 | 5048.0398 | 4984.0296 | 4962.4486 |
| 2.3354 | 5001.4100 | 4953.1691 | 4929.8960 |
| 2.3464 | 4963.4454 | 4922.5738 | 4897.3434 |
| 2.3574 | 5063.2291 | 4892.3057 | 4864.7907 |
| 2.3684 | 4981.5103 | 4862.4412 | 4832.2381 |
| 2.3794 | 4904.3009 | 4833.0030 | 4799.6855 |
| 2.3904 | 4841.4036 | 4804.1991 | 4767.0242 |
| 2.4014 | 4801.1416 | 4776.0559 | 4734.3630 |
| 2.4124 | 4808.0541 | 4748.7852 | 4701.7017 |
| 2.4234 | 4883.0187 | 4722.5433 | 4669.0405 |
| 2.4344 | 4800.7434 | 4697.4972 | 4636.3792 |
| 2.4454 | 4708.2537 | 4673.8182 | 4603.7179 |
| 2.4564 | 4640.5669 | 4651.6746 | 4571.0567 |
| 2.4674 | 4613.8967 | 4631.2218 | 4538.3954 |
| 2.4784 | 4624.8668 | 4612.5910 | 4505.7342 |
| 2.4894 | 4608.8377 | 4595.8764 | 4473.0729 |
| 2.5004 | 4505.5841 | 4581.1213 | 4440.4117 |
| 2.5114 | 4560.6391 | 4568.3032 | 4407.7504 |
| 2.5224 | 4573.2999 | 4557.3180 | 4375.0891 |
| 2.5334 | 4500.0413 | 4547.9622 | 4342.4279 |
| 2.5444 | 4550.6578 | 4539.9131 | 4309.7666 |
| 2.5554 | 4497.6716 | 4532.7050 | 4277.1054 |
| 2.5664 | 4426.5973 | 4525.7055 | 4244.4441 |
| 2.5774 | 4423.5565 | 4518.0938 | 4211.7828 |
| 2.5884 | 4434.1200 | 4508.8560 | 4179.1216 |
| 2.5994 | 4443.6460 | 4496.8158 | 4146.4603 |
| 2.6104 | 4398.0034 | 4480.7217 | 4113.7991 |
| 2.6214 | 4296.5339 | 4459.3991 | 4081.1378 |
| 2.6324 | 4214.7611 | 4431.9479 | 4048.4766 |
| 2.6434 | 4253.4563 | 4397.9271 | 4015.8153 |
| 2.6544 | 4265.3972 | 4357.4548 | 3983.1540 |
| 2.6654 | 4215.2773 | 4311.1803 | 3950.4928 |
| 2.6764 | 4190.0029 | 4260.1411 | 3917.8315 |
| 2.6874 | 4071.9312 | 4205.5642 | 3885.1703 |
| 2.6984 | 4084.0089 | 4148.6837 | 3852.5090 |
| 2.7094 | 3991.0187 | 4090.6151 | 3819.8477 |
| 2.7204 | 3910.8692 | 4032.2934 | 3787.1865 |
| 2.7314 | 3939.3717 | 3974.4604 | 3754.5252 |
| 2.7424 | 3872.4144 | 3917.6772 | 3721.8640 |
| 2.7534 | 3824.2399 | 3862.2785 | 3689.2027 |
| 2.7644 | 3741.6726 | 3808.6355 | 3656.4328 |
| 2.7754 | 3711.6529 | 3756.8092 | 3623.6629 |
| 2.7864 | 3689.8014 | 3706.9377 | 3590.8930 |
| 2.7974 | 3617.0885 | 3659.0147 | 3558.1231 |
| 2.8084 | 3606.2055 | 3612.9744 | 3525.3532 |
| 2.8194 | 3572.3471 | 3568.7058 | 3492.5834 |
| 2.8304 | 3420.5855 | 3526.0664 | 3459.8135 |
| 2.8414 | 3448.1672 | 3484.8944 | 3427.0436 |
| 2.8524 | 3368.6622 | 3445.0191 | 3394.2737 |
| 2.8634 | 3260.4602 | 3406.2702 | 3361.5038 |
| 2.8744 | 3295.8107 | 3368.4845 | 3328.7339 |
| 2.8854 | 3351.0806 | 3331.5112 | 3295.9640 |
| 2.8964 | 3346.0265 | 3295.2144 | 3263.1941 |
| 2.9074 | 3137.0226 | 3259.4753 | 3230.4242 |
| 2.9184 | 3265.2340 | 3224.1922 | 3197.6543 |
| 2.9294 | 3223.3923 | 3189.2797 | 3164.8844 |
| 2.9404 | 3085.5079 | 3155.5303 | 3132.1145 |
| 2.9514 | 3074.7719 | 3121.6496 | 3100.6956 |
| 2.9624 | 3069.1283 | 3088.8291 | 3069.2767 |
| 2.9734 | 3037.6342 | 3056.1700 | 3037.8578 |
| 2.9844 | 2966.6573 | 3023.6437 | 3006.4388 |
| 2.9954 | 2961.1062 | 2991.2280 | 2975.0199 |
| 3.0064 | 2848.6775 | 2958.9053 | 2943.6010 |
| 3.0174 | 2765.3697 | 2926.6620 | 2912.1821 |
| 3.0284 | 2824.7198 | 2894.4871 | 2880.7631 |
| 3.0394 | 2837.9892 | 2862.3720 | 2849.3442 |
| 3.0504 | 2781.7910 | 2830.3097 | 2817.9253 |
| 3.0614 | 2749.4189 | 2798.2943 | 2786.5064 |
| 3.0724 | 2760.3864 | 2766.3210 | 2755.0874 |
| 3.0834 | 2726.6834 | 2734.3858 | 2723.6685 |
| 3.0944 | 2661.0265 | 2702.4851 | 2692.2496 |
| 3.1054 | 2625.2291 | 2670.6158 | 2660.8307 |
| 3.1164 | 2627.2070 | 2638.7752 | 2629.4117 |
| 3.1274 | 2611.7197 | 2617.3063 | 2597.9928 |
| 3.1384 | 2558.1917 | 2591.3614 | 2582.3947 |
| 3.1494 | 2579.8004 | 2575.4203 | 2566.7966 |
| 3.1604 | 2581.0383 | 2559.6742 | 2551.1984 |
| 3.1714 | 2525.4110 | 2544.3040 | 2535.6003 |
| 3.1824 | 2558.4066 | 2528.5106 | 2520.0022 |
| 3.1934 | 2489.8407 | 2512.9123 | 2504.4040 |
| 3.2044 | 2466.9917 | 2497.0639 | 2488.8059 |
| 3.2154 | 2512.1190 | 2481.2297 | 2473.2078 |
| 3.2264 | 2457.9779 | 2465.4087 | 2457.6096 |
| 3.2374 | 2420.4297 | 2449.5999 | 2442.0115 |
| 3.2484 | 2415.5556 | 2433.8026 | 2426.4134 |
| 3.2594 | 2459.0236 | 2418.0160 | 2410.8152 |
| 3.2704 | 2417.6622 | 2402.2394 | 2395.2171 |
| 3.2814 | 2385.4278 | 2386.4721 | 2379.6190 |
| 3.2924 | 2371.2832 | 2370.7137 | 2364.0208 |
| 3.3034 | 2312.2262 | 2354.9635 | 2348.4227 |
| 3.3144 | 2393.7866 | 2339.2211 | 2332.8246 |
| 3.3254 | 2356.8879 | 2323.4860 | 2317.2265 |
| 3.3364 | 2243.5624 | 2307.7577 | 2301.6283 |
| 3.3474 | 2219.0020 | 2292.0360 | 2286.0302 |
| 3.3584 | 2209.8348 | 2276.3203 | 2270.4321 |
| 3.3694 | 2227.1082 | 2260.6104 | 2254.8339 |
| 3.3804 | 2255.9730 | 2244.9060 | 2239.2358 |
| 3.3914 | 2202.1947 | 2229.2067 | 2223.6377 |
| 3.4024 | 2124.3908 | 2213.5123 | 2208.0395 |
| 3.4134 | 2103.7198 | 2197.8226 | 2192.4414 |
| 3.4244 | 2125.4941 | 2182.1372 | 2176.8433 |
| 3.4354 | 2153.7503 | 2166.4560 | 2161.2451 |
| 3.4464 | 2138.5949 | 2150.7788 | 2145.6470 |
| 3.4574 | 2128.6018 | 2135.1054 | 2130.0489 |
| 3.4684 | 2071.7025 | 2119.4356 | 2114.4508 |
| 3.4794 | 2085.5251 | 2103.7692 | 2098.8526 |
| 3.4904 | 2080.3540 | 2088.1061 | 2083.2545 |
| 3.5014 | 2119.0698 | 2075.0807 | 2067.6564 |
| 3.5124 | 2037.9478 | 2060.9147 | 2056.1839 |
| 3.5234 | 1990.0885 | 2049.3862 | 2044.7115 |
| 3.5344 | 1991.7085 | 2037.8605 | 2033.2390 |
| 3.5454 | 2060.4710 | 2026.3373 | 2021.7666 |
| 3.5564 | 2066.4749 | 2014.8167 | 2010.2941 |
| 3.5674 | 1980.7404 | 2003.2985 | 1998.8217 |
| 3.5784 | 1909.3004 | 1991.7826 | 1987.3492 |
| 3.5894 | 1924.2566 | 1980.2689 | 1975.8768 |
| 3.6004 | 1998.7050 | 1968.7573 | 1964.4044 |
| 3.6114 | 1969.3304 | 1957.2478 | 1952.9319 |
| 3.6224 | 1914.2404 | 1945.7403 | 1941.4595 |
| 3.6334 | 1940.0393 | 1934.2347 | 1929.9870 |
| 3.6444 | 1982.0860 | 1922.7310 | 1918.5146 |
| 3.6554 | 1926.5693 | 1911.2290 | 1907.0421 |
| 3.6664 | 1896.1691 | 1899.7288 | 1895.5697 |
| 3.6774 | 1888.6588 | 1888.2303 | 1884.0972 |
| 3.6884 | 1842.2124 | 1878.4213 | 1872.6248 |
| 3.6994 | 1913.6755 | 1867.8812 | 1863.7955 |
| 3.7104 | 1834.2989 | 1859.0305 | 1854.9663 |
| 3.7214 | 1835.0914 | 1850.1814 | 1846.1370 |
| 3.7324 | 1862.0315 | 1841.3337 | 1837.3078 |
| 3.7434 | 1883.7817 | 1832.4874 | 1828.4785 |
| 3.7544 | 1825.8348 | 1823.6424 | 1819.6493 |
| 3.7654 | 1857.7965 | 1814.7988 | 1810.8200 |
| 3.7764 | 1833.5496 | 1805.9565 | 1801.9908 |
| 3.7874 | 1784.4336 | 1797.1155 | 1793.1615 |
| 3.7984 | 1847.8176 | 1788.2758 | 1784.3323 |
| 3.8094 | 1793.5998 | 1779.4373 | 1775.5030 |
| 3.8204 | 1708.3540 | 1770.5999 | 1766.6738 |
| 3.8314 | 1790.4838 | 1761.7638 | 1757.8445 |
| 3.8424 | 1801.7896 | 1752.9288 | 1749.0152 |
| 3.8534 | 1790.7315 | 1744.0950 | 1740.1860 |
| 3.8644 | 1686.4631 | 1735.2623 | 1731.3567 |
| 3.8754 | 1696.5634 | 1729.0264 | 1722.5275 |
| 3.8864 | 1743.9159 | 1721.6648 | 1717.7629 |
| 3.8974 | 1741.5064 | 1716.9001 | 1712.9984 |
| 3.9084 | 1660.2527 | 1712.1365 | 1708.2338 |
| 3.9194 | 1669.9027 | 1707.3739 | 1703.4692 |
| 3.9304 | 1707.0762 | 1702.6123 | 1698.7047 |
| 3.9414 | 1644.0806 | 1697.8519 | 1693.9401 |
| 3.9524 | 1668.1593 | 1693.0924 | 1689.1755 |
| 3.9634 | 1680.5585 | 1688.3340 | 1684.4109 |
| 3.9744 | 1664.5973 | 1683.5767 | 1679.6464 |
| 3.9854 | 1650.6460 | 1678.8203 | 1674.8818 |
| 3.9964 | 1675.4051 | 1674.0651 | 1670.1172 |
| 4.0074 | 1659.2085 | 1669.3108 | 1665.3527 |
| 4.0184 | 1648.7448 | 1664.5576 | 1660.5881 |
| 4.0294 | 1645.1072 | 1659.8054 | 1655.8235 |
| 4.0404 | 1620.0000 | 1655.0543 | 1651.0590 |
| 4.0514 | 1631.1593 | 1650.3042 | 1646.2944 |
| 4.0624 | 1665.2670 | 1645.6560 | 1641.5298 |
| 4.0734 | 1648.6175 | 1640.9651 | 1636.9231 |
| 4.0844 | 1608.0708 | 1636.3761 | 1632.3164 |
| 4.0954 | 1657.5998 | 1631.7882 | 1627.7097 |
| 4.1064 | 1639.5187 | 1627.2014 | 1623.1030 |
| 4.1174 | 1615.6106 | 1622.6157 | 1618.4963 |
| 4.1284 | 1574.0035 | 1618.0311 | 1613.8896 |
| 4.1394 | 1615.6096 | 1613.4477 | 1609.2829 |
| 4.1504 | 1586.6283 | 1608.8654 | 1604.6762 |
| 4.1614 | 1567.1298 | 1604.2843 | 1600.0695 |
| 4.1724 | 1611.0236 | 1599.7044 | 1595.4628 |
| 4.1834 | 1569.7788 | 1595.1258 | 1590.8561 |
| 4.1944 | 1585.8653 | 1590.5484 | 1586.2493 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 8 Etosha22 crt 0-0.1cm S1 glycolated | 2.0054 | 29.9894 | 0.0110 | 12/5/2023 8:57:52 AM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.6335 | 343.22 | 0.2165 | 33.52097 | 45.51 |
| 5.2881 | 261.22 | 0.2165 | 16.69823 | 34.63 |
| 7.0649 | 754.24 | 0.3897 | 12.50204 | 100.00 |
| 8.7236 | 230.24 | 0.3464 | 10.12824 | 30.53 |
| 15.7242 | 340.19 | 0.0866 | 5.63129 | 45.10 |
| 17.6261 | 31.62 | 0.2598 | 5.02771 | 4.19 |
| 18.1555 | 51.02 | 0.1299 | 4.88229 | 6.76 |
| 19.6757 | 40.20 | 0.4330 | 4.50836 | 5.33 |
| 25.8989 | 328.46 | 0.0758 | 3.43744 | 43.55 |
| 26.7182 | 65.48 | 0.3031 | 3.33386 | 8.68 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-016-6876 | 34 | Potassium Calcium Manganese Aluminum Silicate Hydroxide Hydrate | K0.38 Ca0.12 Mn2 Al0.62 Si2.71 O8 ( O H )1.33 ( H2 O )1.75 | Ganophyllite | 20 |
| * | 04-017-4317 | 26 | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | K Mg0.2 Mn0.1 Fe2.4 Al1.7 Si2.6 O10 ( O H )2 | Biotite-1M | 17 |
| * | 01-075-8323 | 10 | Magnesium Silicate Hydroxide Hydrate | Mg8 ( Si12 O30 ( O H )4 ) ( H2 O )11.82 | Sepiolite | 10 |
| * | 04-011-6753 | 25 | Sodium Aluminum Silicate Hydrate | Na8 Al8 Si16 O48 ( H2 O )8 | Analcime | 22 |
| * | 04-025-4215 | 9 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 31 |

Anchor Scan Parameters

Dataset Name	8 Etosha22 crt 0-0.1cm S1 glycolated

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 8\8 Etosha22 crt 0-0.1cm S1 glycolated.xrdml

Sample Identification	8 Etosha22 crt 0-0.1cm S1 glycolated

Measurement Start Date/Time	12/5/2023 8:57:52 AM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes