8 Etosha 22 CRT 0-0.1 cm S1 REGULAR

Graphics

Graphics

Graphics

Quantitative Results

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	12.0

Phase Potassium Manganese Aluminum Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	23.0

Phase Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide

Weight fraction/ %	13.0

Phase Magnesium Silicate Hydroxide Hydrate

Weight fraction/ %	22.0

Phase Copper Arsenate Chloride Hydroxide Hydrate

Weight fraction/ %	5.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	26.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Sodium Aluminum Silicate Hydrate | Potassium Manganese Aluminum Silicon Oxide Hydroxide Hydrate | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | Magnesium Silicate Hydroxide Hydrate | Copper Arsenate Chloride Hydroxide Hydrate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide |
| --- | --- | --- | --- | --- | --- | --- |
| 8 Etosha22 CRT 0-0.1cm S1 | 12.0 | 23.0 | 13.0 | 22.0 | 5.0 | 26.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 5778.0000 | 5791.6295 | 5778.0000 |
| 2.0164 | 5658.7665 | 5754.1729 | 5738.6094 |
| 2.0274 | 5641.8191 | 5715.3004 | 5699.2188 |
| 2.0384 | 5711.4926 | 5676.4578 | 5659.8281 |
| 2.0494 | 5642.1652 | 5637.6482 | 5620.4375 |
| 2.0604 | 5561.3628 | 5598.8751 | 5581.0469 |
| 2.0714 | 5470.9882 | 5560.1425 | 5541.6563 |
| 2.0824 | 5610.2906 | 5521.4551 | 5502.2656 |
| 2.0934 | 5617.9036 | 5482.8180 | 5462.8750 |
| 2.1044 | 5547.9513 | 5444.2373 | 5423.4844 |
| 2.1154 | 5426.2734 | 5405.7199 | 5384.0938 |
| 2.1264 | 5362.7832 | 5367.2735 | 5344.7031 |
| 2.1374 | 5329.0413 | 5328.9070 | 5305.3125 |
| 2.1484 | 5210.7970 | 5290.6304 | 5265.9219 |
| 2.1594 | 5348.4031 | 5252.4547 | 5226.5313 |
| 2.1704 | 5194.5693 | 5214.3927 | 5187.1407 |
| 2.1814 | 5139.2802 | 5176.4582 | 5147.7500 |
| 2.1924 | 5102.8663 | 5138.9776 | 5108.3594 |
| 2.2034 | 5048.6195 | 5109.5236 | 5077.4574 |
| 2.2144 | 5082.4970 | 5080.5591 | 5046.5554 |
| 2.2254 | 5070.5084 | 5051.7933 | 5015.6535 |
| 2.2364 | 5062.5472 | 5023.2478 | 4984.7515 |
| 2.2474 | 5015.3373 | 4994.9461 | 4953.8495 |
| 2.2584 | 4979.2734 | 4966.9127 | 4922.9475 |
| 2.2694 | 5040.6372 | 4939.1736 | 4892.0455 |
| 2.2804 | 4933.3127 | 4911.7560 | 4861.1435 |
| 2.2914 | 4945.4523 | 4884.6877 | 4830.2415 |
| 2.3024 | 4992.9823 | 4857.9971 | 4799.3396 |
| 2.3134 | 4936.6440 | 4831.7130 | 4768.4376 |
| 2.3244 | 4808.6534 | 4805.8636 | 4737.5356 |
| 2.3354 | 4821.8614 | 4780.4766 | 4706.6336 |
| 2.3464 | 4817.5634 | 4755.5785 | 4675.7316 |
| 2.3574 | 4732.8407 | 4731.1939 | 4644.8296 |
| 2.3684 | 4759.2670 | 4707.3448 | 4613.9276 |
| 2.3794 | 4803.6726 | 4684.0456 | 4583.0257 |
| 2.3904 | 4725.7021 | 4661.1945 | 4551.9921 |
| 2.4014 | 4618.7876 | 4638.9193 | 4520.9585 |
| 2.4124 | 4580.2861 | 4617.2304 | 4489.9250 |
| 2.4234 | 4628.8800 | 4596.1274 | 4458.8914 |
| 2.4344 | 4644.1239 | 4575.6030 | 4427.8578 |
| 2.4454 | 4653.7827 | 4555.6424 | 4396.8243 |
| 2.4564 | 4577.2999 | 4536.2221 | 4365.7907 |
| 2.4674 | 4517.9086 | 4517.3094 | 4334.7571 |
| 2.4784 | 4578.2965 | 4498.8611 | 4303.7236 |
| 2.4894 | 4534.4503 | 4480.8223 | 4272.6900 |
| 2.5004 | 4486.3805 | 4463.1255 | 4241.6564 |
| 2.5114 | 4422.2379 | 4445.6891 | 4210.6229 |
| 2.5224 | 4425.8117 | 4428.4162 | 4179.5893 |
| 2.5334 | 4366.5752 | 4411.1930 | 4148.5558 |
| 2.5444 | 4253.0462 | 4393.8882 | 4117.5222 |
| 2.5554 | 4291.7571 | 4376.3520 | 4086.4886 |
| 2.5664 | 4317.3289 | 4358.4161 | 4055.4551 |
| 2.5774 | 4288.8260 | 4339.8953 | 4024.4215 |
| 2.5884 | 4242.8230 | 4320.5896 | 3993.3879 |
| 2.5994 | 4230.6372 | 4300.2894 | 3962.3544 |
| 2.6104 | 4240.0841 | 4278.7820 | 3931.3208 |
| 2.6214 | 4196.1957 | 4255.8604 | 3900.2872 |
| 2.6324 | 4189.0118 | 4231.3336 | 3869.2537 |
| 2.6434 | 4078.0875 | 4205.0382 | 3838.2201 |
| 2.6544 | 4007.7945 | 4176.8493 | 3807.1865 |
| 2.6654 | 4038.8230 | 4146.6892 | 3776.1530 |
| 2.6764 | 3927.7910 | 4114.5337 | 3745.1194 |
| 2.6874 | 3940.8673 | 4080.4140 | 3714.0858 |
| 2.6984 | 3933.2212 | 4044.4139 | 3683.0523 |
| 2.7094 | 3848.1239 | 4006.6639 | 3652.0187 |
| 2.7204 | 3838.9838 | 3967.3315 | 3620.9851 |
| 2.7314 | 3720.3186 | 3926.6100 | 3589.9516 |
| 2.7424 | 3756.2330 | 3884.7078 | 3558.9180 |
| 2.7534 | 3734.0610 | 3841.8325 | 3527.8845 |
| 2.7644 | 3643.8879 | 3798.0766 | 3496.7193 |
| 2.7754 | 3577.3776 | 3753.7546 | 3465.5542 |
| 2.7864 | 3603.9066 | 3709.0548 | 3434.3890 |
| 2.7974 | 3586.8761 | 3664.1433 | 3403.2239 |
| 2.8084 | 3557.9798 | 3619.1675 | 3372.0587 |
| 2.8194 | 3469.5034 | 3574.2565 | 3340.8936 |
| 2.8304 | 3356.8333 | 3529.5219 | 3309.7284 |
| 2.8414 | 3305.9646 | 3485.0586 | 3278.5633 |
| 2.8524 | 3371.1416 | 3440.9464 | 3247.3981 |
| 2.8634 | 3236.9469 | 3397.2512 | 3216.2330 |
| 2.8744 | 3264.0138 | 3354.0263 | 3185.0679 |
| 2.8854 | 3155.8554 | 3311.3137 | 3153.9027 |
| 2.8964 | 3226.6770 | 3269.1447 | 3122.7376 |
| 2.9074 | 3026.4169 | 3227.5419 | 3091.5724 |
| 2.9184 | 3078.4759 | 3186.5189 | 3060.4073 |
| 2.9294 | 3048.9115 | 3146.0821 | 3029.2421 |
| 2.9404 | 2930.4897 | 3106.3053 | 2998.0770 |
| 2.9514 | 3005.1711 | 3068.8730 | 2968.8246 |
| 2.9624 | 2998.6416 | 3032.0829 | 2939.5722 |
| 2.9734 | 2869.4907 | 2995.8453 | 2910.3198 |
| 2.9844 | 2833.0049 | 2960.1407 | 2881.0674 |
| 2.9954 | 2861.4690 | 2924.9467 | 2851.8150 |
| 3.0064 | 2851.3127 | 2890.2382 | 2822.5626 |
| 3.0174 | 2802.1996 | 2855.9888 | 2793.3102 |
| 3.0284 | 2744.6962 | 2822.1707 | 2764.0578 |
| 3.0394 | 2673.1750 | 2788.7554 | 2734.8054 |
| 3.0504 | 2690.3648 | 2755.7143 | 2705.5530 |
| 3.0614 | 2697.2065 | 2723.0190 | 2676.3006 |
| 3.0724 | 2609.1146 | 2690.6417 | 2647.0482 |
| 3.0834 | 2656.2459 | 2658.5554 | 2617.7958 |
| 3.0944 | 2751.8805 | 2626.7344 | 2588.5434 |
| 3.1054 | 2556.1052 | 2595.1541 | 2559.2911 |
| 3.1164 | 2531.4130 | 2563.7914 | 2530.0387 |
| 3.1274 | 2478.7640 | 2533.1932 | 2500.7863 |
| 3.1384 | 2457.8638 | 2516.3345 | 2486.2341 |
| 3.1494 | 2520.3127 | 2500.2019 | 2471.6820 |
| 3.1604 | 2498.7168 | 2484.2103 | 2457.1298 |
| 3.1714 | 2489.7148 | 2468.3444 | 2442.5777 |
| 3.1824 | 2437.9631 | 2452.5905 | 2428.0256 |
| 3.1934 | 2469.1416 | 2436.9361 | 2413.4734 |
| 3.2044 | 2432.9562 | 2421.3703 | 2398.9213 |
| 3.2154 | 2399.6323 | 2405.8832 | 2384.3692 |
| 3.2264 | 2398.7065 | 2390.4661 | 2369.8170 |
| 3.2374 | 2417.0364 | 2375.1113 | 2355.2649 |
| 3.2484 | 2432.1666 | 2359.8122 | 2340.7128 |
| 3.2594 | 2333.3304 | 2344.5628 | 2326.1606 |
| 3.2704 | 2314.5388 | 2329.3579 | 2311.6085 |
| 3.2814 | 2293.7207 | 2314.1929 | 2297.0563 |
| 3.2924 | 2244.9513 | 2299.0641 | 2282.5042 |
| 3.3034 | 2240.0855 | 2283.9677 | 2267.9521 |
| 3.3144 | 2261.4130 | 2268.9010 | 2253.3999 |
| 3.3254 | 2285.4543 | 2253.8613 | 2238.8478 |
| 3.3364 | 2283.7458 | 2238.8462 | 2224.2957 |
| 3.3474 | 2320.4936 | 2223.8538 | 2209.7435 |
| 3.3584 | 2296.2920 | 2208.8822 | 2195.1914 |
| 3.3694 | 2227.1691 | 2193.9300 | 2180.6392 |
| 3.3804 | 2163.6445 | 2178.9957 | 2166.0871 |
| 3.3914 | 2164.6903 | 2164.0781 | 2151.5350 |
| 3.4024 | 2167.0492 | 2149.1762 | 2136.9828 |
| 3.4134 | 2107.7129 | 2134.2888 | 2122.4307 |
| 3.4244 | 2087.4676 | 2119.4153 | 2107.8786 |
| 3.4354 | 2120.9135 | 2104.5546 | 2093.3264 |
| 3.4464 | 2119.9164 | 2089.7061 | 2078.7743 |
| 3.4574 | 2071.0324 | 2074.8692 | 2064.2221 |
| 3.4684 | 2029.5934 | 2060.0432 | 2049.6700 |
| 3.4794 | 2011.2360 | 2045.2275 | 2035.1179 |
| 3.4904 | 2032.7124 | 2030.4216 | 2020.5657 |
| 3.5014 | 1995.6312 | 2015.8059 | 2006.0136 |
| 3.5124 | 1983.9936 | 2005.5122 | 1996.1363 |
| 3.5234 | 2012.2773 | 1995.4078 | 1986.2589 |
| 3.5344 | 2057.4228 | 1985.3114 | 1976.3816 |
| 3.5454 | 1940.8239 | 1975.2227 | 1966.5043 |
| 3.5564 | 1941.3127 | 1965.1412 | 1956.6269 |
| 3.5674 | 1910.8082 | 1955.0668 | 1946.7496 |
| 3.5784 | 1878.0900 | 1944.9991 | 1936.8723 |
| 3.5894 | 1942.2921 | 1934.9377 | 1926.9949 |
| 3.6004 | 2008.3678 | 1924.8824 | 1917.1176 |
| 3.6114 | 1951.0845 | 1914.8329 | 1907.2403 |
| 3.6224 | 1923.3186 | 1904.7891 | 1897.3629 |
| 3.6334 | 1935.7434 | 1894.7505 | 1887.4856 |
| 3.6444 | 1822.6086 | 1884.7171 | 1877.6083 |
| 3.6554 | 1864.8053 | 1874.6887 | 1867.7309 |
| 3.6664 | 1852.1775 | 1864.6649 | 1857.8536 |
| 3.6774 | 1886.2026 | 1854.6456 | 1847.9763 |
| 3.6884 | 1766.9646 | 1844.6768 | 1838.0989 |
| 3.6994 | 1879.4592 | 1835.8107 | 1829.4123 |
| 3.7104 | 1828.0216 | 1826.9946 | 1820.7257 |
| 3.7214 | 1752.1947 | 1818.1824 | 1812.0391 |
| 3.7324 | 1808.2896 | 1809.3739 | 1803.3525 |
| 3.7434 | 1779.0885 | 1800.5690 | 1794.6658 |
| 3.7544 | 1863.8393 | 1791.7675 | 1785.9792 |
| 3.7654 | 1770.3766 | 1782.9692 | 1777.2926 |
| 3.7764 | 1775.8097 | 1774.1742 | 1768.6060 |
| 3.7874 | 1786.9027 | 1765.3821 | 1759.9194 |
| 3.7984 | 1737.9002 | 1756.5930 | 1751.2327 |
| 3.8094 | 1709.1731 | 1747.8068 | 1742.5461 |
| 3.8204 | 1718.9351 | 1739.0232 | 1733.8595 |
| 3.8314 | 1683.7739 | 1730.2423 | 1725.1729 |
| 3.8424 | 1726.4735 | 1721.4640 | 1716.4863 |
| 3.8534 | 1735.3894 | 1712.6880 | 1707.7997 |
| 3.8644 | 1736.5231 | 1703.9145 | 1699.1130 |
| 3.8754 | 1682.4631 | 1695.2294 | 1690.4264 |
| 3.8864 | 1669.9779 | 1688.6030 | 1683.9687 |
| 3.8974 | 1618.3796 | 1682.0650 | 1677.5110 |
| 3.9084 | 1706.4548 | 1675.5290 | 1671.0533 |
| 3.9194 | 1751.7610 | 1668.9950 | 1664.5956 |
| 3.9304 | 1698.2084 | 1662.4630 | 1658.1379 |
| 3.9414 | 1616.7955 | 1655.9327 | 1651.6802 |
| 3.9524 | 1633.5472 | 1649.4043 | 1645.2225 |
| 3.9634 | 1666.1829 | 1642.8776 | 1638.7648 |
| 3.9744 | 1639.7930 | 1636.3526 | 1632.3071 |
| 3.9854 | 1578.7522 | 1629.8293 | 1625.8494 |
| 3.9964 | 1569.7404 | 1623.3074 | 1619.3917 |
| 4.0074 | 1582.3363 | 1616.7872 | 1612.9340 |
| 4.0184 | 1558.4690 | 1610.2684 | 1606.4763 |
| 4.0294 | 1590.2616 | 1603.7510 | 1600.0187 |
| 4.0404 | 1603.3230 | 1597.2350 | 1593.5610 |
| 4.0514 | 1622.8377 | 1590.7204 | 1587.1033 |
| 4.0624 | 1590.0000 | 1584.2030 | 1580.6456 |
| 4.0734 | 1552.7138 | 1577.5898 | 1574.0826 |
| 4.0844 | 1495.8407 | 1570.9737 | 1567.5197 |
| 4.0954 | 1524.5172 | 1564.3588 | 1560.9567 |
| 4.1064 | 1497.9838 | 1557.7450 | 1554.3938 |
| 4.1174 | 1573.9499 | 1551.1324 | 1547.8308 |
| 4.1284 | 1595.8766 | 1544.5209 | 1541.2679 |
| 4.1394 | 1537.6932 | 1537.9104 | 1534.7049 |
| 4.1504 | 1540.3481 | 1531.3010 | 1528.1420 |
| 4.1614 | 1541.4100 | 1524.6926 | 1521.5791 |
| 4.1724 | 1519.3092 | 1518.0851 | 1515.0161 |
| 4.1834 | 1499.9292 | 1511.4786 | 1508.4532 |
| 4.1944 | 1486.2030 | 1504.8730 | 1501.8902 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 8 Etosha22 CRT 0-0.1cm S1 | 2.0054 | 29.9894 | 0.0110 | 12/1/2023 11:17:45 AM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.6625 | 330.58 | 0.3897 | 33.15540 | 27.93 |
| 7.0714 | 1183.80 | 0.1299 | 12.49058 | 100.00 |
| 8.6832 | 238.94 | 0.2165 | 10.17534 | 20.18 |
| 12.9562 | 22.65 | 0.5196 | 6.82745 | 1.91 |
| 15.7348 | 278.76 | 0.1299 | 5.62753 | 23.55 |
| 18.1830 | 48.95 | 0.1299 | 4.87494 | 4.13 |
| 19.7147 | 32.32 | 0.4330 | 4.49953 | 2.73 |
| 25.8971 | 302.20 | 0.0541 | 3.43767 | 25.53 |
| 26.7004 | 57.76 | 0.2598 | 3.33604 | 4.88 |
| 27.4961 | 27.21 | 0.2598 | 3.24128 | 2.30 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 01-072-4625 | 32 | Sodium Aluminum Silicate Hydrate | Na Al ( Si2 O6 ) ( H2 O ) | Analcime | 12 |
| * | 04-017-7286 | 49 | Potassium Manganese Aluminum Silicon Oxide Hydroxide Hydrate | K0.8 Mn4 Al1.08 Si4.92 O16 ( O H )2 ( H2 O )3 | Ganophyllite | 23 |
| * | 04-017-4317 | 26 | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | K Mg0.2 Mn0.1 Fe2.4 Al1.7 Si2.6 O10 ( O H )2 | Biotite-1M | 13 |
| * | 01-080-5017 | 17 | Magnesium Silicate Hydroxide Hydrate | Mg7.73 ( Si12 O30 ) ( O H )4 ( H2 O )4 ( H2 O )6 | Sepiolite | 22 |
| * | 01-083-3890 | 18 | Copper Arsenate Chloride Hydroxide Hydrate | Cu10 ( As O4 )2 ( Cl0.9 ( O H )13.1 ) ( H2 O )4.3 | Parnauite | 5 |
| * | 04-025-4215 | 13 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 26 |

Anchor Scan Parameters

Dataset Name	8 Etosha22 CRT 0-0.1cm S1

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 8\8 Etosha22 CRT 0-0.1cm S1.xrdml

Sample Identification	8 Etosha22 CRT 0-0.1cm S1

Measurement Start Date/Time	12/1/2023 11:17:45 AM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes