9 Etosha 22 Sub 0.1-4 cm S1 400 C

Graphics

Graphics

Graphics

Quantitative Results

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	23.0

Phase Potassium Magnesium Aluminum Silicate Hydroxide

Weight fraction/ %	22.0

Phase Magnesium Silicate Hydroxide Hydrate

Weight fraction/ %	21.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	34.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Sodium Aluminum Silicate Hydrate | Potassium Magnesium Aluminum Silicate Hydroxide | Magnesium Silicate Hydroxide Hydrate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide |
| --- | --- | --- | --- | --- |
| 9 Etosha22 Sub 0.1-4cm S1 heat 400C | 23.0 | 22.0 | 21.0 | 34.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 5381.0000 | 5369.3558 | 5381.0000 |
| 2.0164 | 5324.5128 | 5340.0549 | 5340.0549 |
| 2.0274 | 5203.9430 | 5299.1098 | 5299.1098 |
| 2.0384 | 5160.3407 | 5258.1647 | 5258.1647 |
| 2.0494 | 5110.4612 | 5218.2040 | 5217.2195 |
| 2.0604 | 4992.8496 | 5177.4490 | 5176.2744 |
| 2.0714 | 5130.2861 | 5137.0018 | 5135.3293 |
| 2.0824 | 5153.4936 | 5096.1569 | 5094.3842 |
| 2.0934 | 5081.1357 | 5055.2193 | 5053.4391 |
| 2.1044 | 4964.8407 | 5014.2818 | 5012.4940 |
| 2.1154 | 5039.9548 | 4973.3443 | 4971.5489 |
| 2.1264 | 4950.2144 | 4932.4069 | 4930.6038 |
| 2.1374 | 4928.6549 | 4891.4696 | 4889.6586 |
| 2.1484 | 4932.4956 | 4850.5322 | 4848.7135 |
| 2.1594 | 4866.3215 | 4809.5950 | 4807.7684 |
| 2.1704 | 4824.4351 | 4768.6578 | 4766.8233 |
| 2.1814 | 4758.2301 | 4727.7206 | 4725.8782 |
| 2.1924 | 4716.1057 | 4691.3601 | 4684.9331 |
| 2.2034 | 4580.9027 | 4661.9394 | 4660.0810 |
| 2.2144 | 4572.5688 | 4637.0955 | 4635.2289 |
| 2.2254 | 4602.6323 | 4612.2515 | 4610.3768 |
| 2.2364 | 4655.8363 | 4587.4076 | 4585.5247 |
| 2.2474 | 4611.7807 | 4562.5638 | 4560.6726 |
| 2.2584 | 4601.5020 | 4537.7200 | 4535.8205 |
| 2.2694 | 4611.8053 | 4512.8763 | 4510.9684 |
| 2.2804 | 4588.0890 | 4488.0326 | 4486.1163 |
| 2.2914 | 4529.9715 | 4463.1890 | 4461.2642 |
| 2.3024 | 4450.6593 | 4438.3455 | 4436.4121 |
| 2.3134 | 4467.4218 | 4413.5020 | 4411.5600 |
| 2.3244 | 4445.9498 | 4388.6585 | 4386.7079 |
| 2.3354 | 4395.2920 | 4363.8152 | 4361.8558 |
| 2.3464 | 4438.7591 | 4338.9718 | 4337.0037 |
| 2.3574 | 4380.1750 | 4314.1286 | 4312.1516 |
| 2.3684 | 4293.1180 | 4289.2854 | 4287.2995 |
| 2.3794 | 4276.2675 | 4264.4422 | 4262.4475 |
| 2.3904 | 4286.1436 | 4239.5991 | 4237.5954 |
| 2.4014 | 4248.3894 | 4214.7561 | 4212.7433 |
| 2.4124 | 4249.4474 | 4189.9132 | 4187.8912 |
| 2.4234 | 4205.3776 | 4165.0703 | 4163.0391 |
| 2.4344 | 4154.3879 | 4140.2274 | 4138.1870 |
| 2.4454 | 4115.7758 | 4115.3847 | 4113.3349 |
| 2.4564 | 4031.9769 | 4090.5419 | 4088.4828 |
| 2.4674 | 4009.8791 | 4065.6993 | 4063.6307 |
| 2.4784 | 4035.1445 | 4040.8567 | 4038.7786 |
| 2.4894 | 4015.0511 | 4016.0142 | 4013.9265 |
| 2.5004 | 3986.2168 | 3991.1718 | 3989.0744 |
| 2.5114 | 3965.8692 | 3966.3294 | 3964.2223 |
| 2.5224 | 3959.2232 | 3941.4871 | 3939.3702 |
| 2.5334 | 3930.8112 | 3916.6448 | 3914.5181 |
| 2.5444 | 3894.7276 | 3891.8027 | 3889.6660 |
| 2.5554 | 3830.9921 | 3866.9606 | 3864.8139 |
| 2.5664 | 3833.4764 | 3842.9593 | 3839.9618 |
| 2.5774 | 3845.0521 | 3820.2330 | 3818.0661 |
| 2.5884 | 3815.2458 | 3798.3475 | 3796.1704 |
| 2.5994 | 3811.9558 | 3776.4620 | 3774.2747 |
| 2.6104 | 3808.2119 | 3754.5767 | 3752.3790 |
| 2.6214 | 3733.7935 | 3732.6914 | 3730.4833 |
| 2.6324 | 3653.6593 | 3710.8062 | 3708.5876 |
| 2.6434 | 3675.7729 | 3688.9211 | 3686.6919 |
| 2.6544 | 3590.7507 | 3667.0360 | 3664.7962 |
| 2.6654 | 3560.8496 | 3645.1511 | 3642.9005 |
| 2.6764 | 3617.9823 | 3623.2662 | 3621.0048 |
| 2.6874 | 3547.6027 | 3601.3814 | 3599.1091 |
| 2.6984 | 3559.4912 | 3579.4966 | 3577.2134 |
| 2.7094 | 3506.4965 | 3557.6120 | 3555.3177 |
| 2.7204 | 3440.2660 | 3535.7274 | 3533.4220 |
| 2.7314 | 3477.4838 | 3513.8429 | 3511.5263 |
| 2.7424 | 3443.7075 | 3491.9585 | 3489.6306 |
| 2.7534 | 3503.3707 | 3470.0741 | 3467.7350 |
| 2.7644 | 3494.9498 | 3448.1899 | 3445.8393 |
| 2.7754 | 3406.6834 | 3426.3057 | 3423.9436 |
| 2.7864 | 3297.0069 | 3404.4216 | 3402.0479 |
| 2.7974 | 3407.7788 | 3382.5376 | 3380.1522 |
| 2.8084 | 3346.8368 | 3360.6537 | 3358.2565 |
| 2.8194 | 3336.1809 | 3338.7699 | 3336.3608 |
| 2.8304 | 3349.8274 | 3316.8861 | 3314.4651 |
| 2.8414 | 3189.3972 | 3295.0025 | 3292.5694 |
| 2.8524 | 3248.9808 | 3273.1189 | 3270.6737 |
| 2.8634 | 3289.4307 | 3251.2355 | 3248.7780 |
| 2.8744 | 3205.5526 | 3229.3521 | 3226.8823 |
| 2.8854 | 3116.4710 | 3207.4688 | 3204.9866 |
| 2.8964 | 3245.4204 | 3185.5856 | 3183.0909 |
| 2.9074 | 3153.0944 | 3163.7025 | 3161.1952 |
| 2.9184 | 3163.0850 | 3141.8195 | 3139.2995 |
| 2.9294 | 3071.2655 | 3119.9366 | 3117.4038 |
| 2.9404 | 3107.2999 | 3100.5114 | 3095.5081 |
| 2.9514 | 3072.7109 | 3081.4102 | 3078.8515 |
| 2.9624 | 3100.4454 | 3064.7667 | 3062.1948 |
| 2.9734 | 3094.0610 | 3048.1233 | 3045.5382 |
| 2.9844 | 3096.1401 | 3031.4799 | 3028.8816 |
| 2.9954 | 3001.5310 | 3014.8367 | 3012.2250 |
| 3.0064 | 3008.1327 | 2998.1936 | 2995.5684 |
| 3.0174 | 3021.6460 | 2981.5506 | 2978.9117 |
| 3.0284 | 3003.1386 | 2964.9077 | 2962.2551 |
| 3.0394 | 2970.9302 | 2948.2649 | 2945.5985 |
| 3.0504 | 2905.5974 | 2931.6222 | 2928.9419 |
| 3.0614 | 2976.8436 | 2914.9796 | 2912.2853 |
| 3.0724 | 2911.7748 | 2898.3371 | 2895.6286 |
| 3.0834 | 2859.7719 | 2881.6948 | 2878.9720 |
| 3.0944 | 2890.0000 | 2865.0525 | 2862.3154 |
| 3.1054 | 2864.1111 | 2848.4104 | 2845.6588 |
| 3.1164 | 2789.3112 | 2831.7684 | 2829.0021 |
| 3.1274 | 2822.6726 | 2815.1265 | 2812.3455 |
| 3.1384 | 2811.2557 | 2798.5749 | 2795.6889 |
| 3.1494 | 2806.5821 | 2781.9996 | 2779.0323 |
| 3.1604 | 2808.1652 | 2765.3699 | 2762.3757 |
| 3.1714 | 2834.8357 | 2748.7302 | 2745.7190 |
| 3.1824 | 2651.7817 | 2732.0907 | 2729.0624 |
| 3.1934 | 2670.8053 | 2715.4513 | 2712.4058 |
| 3.2044 | 2680.0905 | 2698.8120 | 2695.7492 |
| 3.2154 | 2650.7758 | 2682.1730 | 2679.0926 |
| 3.2264 | 2661.9440 | 2665.5340 | 2662.4359 |
| 3.2374 | 2684.8319 | 2648.8953 | 2645.7793 |
| 3.2484 | 2645.4444 | 2632.2567 | 2629.1227 |
| 3.2594 | 2614.0118 | 2615.6183 | 2612.4661 |
| 3.2704 | 2618.3461 | 2598.9800 | 2595.8095 |
| 3.2814 | 2571.7207 | 2582.3419 | 2579.1528 |
| 3.2924 | 2548.3584 | 2565.7040 | 2562.4962 |
| 3.3034 | 2547.7138 | 2549.0662 | 2545.8396 |
| 3.3144 | 2514.5197 | 2534.1376 | 2529.1830 |
| 3.3254 | 2546.7994 | 2519.4346 | 2516.1698 |
| 3.3364 | 2482.7895 | 2506.4408 | 2503.1566 |
| 3.3474 | 2442.4690 | 2493.4472 | 2490.1434 |
| 3.3584 | 2455.0634 | 2480.4538 | 2477.1302 |
| 3.3694 | 2439.6205 | 2467.4605 | 2464.1170 |
| 3.3804 | 2425.9085 | 2454.4675 | 2451.1038 |
| 3.3914 | 2438.3363 | 2441.4746 | 2438.0906 |
| 3.4024 | 2466.1706 | 2428.4819 | 2425.0774 |
| 3.4134 | 2446.9233 | 2415.4894 | 2412.0642 |
| 3.4244 | 2471.7449 | 2402.4972 | 2399.0510 |
| 3.4354 | 2404.5526 | 2389.5051 | 2386.0378 |
| 3.4464 | 2410.3850 | 2376.5132 | 2373.0246 |
| 3.4574 | 2374.4631 | 2363.5216 | 2360.0114 |
| 3.4684 | 2312.3058 | 2350.5301 | 2346.9982 |
| 3.4794 | 2352.8781 | 2337.5389 | 2333.9850 |
| 3.4904 | 2336.8053 | 2324.5479 | 2320.9719 |
| 3.5014 | 2298.2104 | 2312.3124 | 2307.9587 |
| 3.5124 | 2290.6839 | 2300.1768 | 2296.5557 |
| 3.5234 | 2279.1652 | 2288.7967 | 2285.1528 |
| 3.5344 | 2298.7960 | 2277.4169 | 2273.7499 |
| 3.5454 | 2301.0718 | 2266.0373 | 2262.3470 |
| 3.5564 | 2230.5604 | 2254.6579 | 2250.9440 |
| 3.5674 | 2246.9931 | 2243.2788 | 2239.5411 |
| 3.5784 | 2228.4223 | 2231.8999 | 2228.1382 |
| 3.5894 | 2298.8407 | 2220.5213 | 2216.7353 |
| 3.6004 | 2285.4543 | 2209.1429 | 2205.3323 |
| 3.6114 | 2209.0570 | 2197.7648 | 2193.9294 |
| 3.6224 | 2165.3761 | 2186.3869 | 2182.5265 |
| 3.6334 | 2199.1347 | 2175.0093 | 2171.1236 |
| 3.6444 | 2133.1770 | 2163.6320 | 2159.7206 |
| 3.6554 | 2213.3334 | 2152.2549 | 2148.3177 |
| 3.6664 | 2147.9729 | 2140.8782 | 2136.9148 |
| 3.6774 | 2171.3343 | 2129.5017 | 2125.5119 |
| 3.6884 | 2118.0044 | 2118.9431 | 2114.1089 |
| 3.6994 | 2081.4297 | 2108.4927 | 2104.4492 |
| 3.7104 | 2049.0364 | 2098.8603 | 2094.7895 |
| 3.7214 | 2096.4572 | 2089.2282 | 2085.1298 |
| 3.7324 | 2196.7586 | 2079.5964 | 2075.4700 |
| 3.7434 | 2199.2901 | 2069.9649 | 2065.8103 |
| 3.7544 | 2005.2817 | 2060.3337 | 2056.1506 |
| 3.7654 | 2077.1918 | 2050.7028 | 2046.4908 |
| 3.7764 | 2049.6553 | 2041.0723 | 2036.8311 |
| 3.7874 | 1992.5044 | 2031.4421 | 2027.1714 |
| 3.7984 | 2085.6834 | 2021.8122 | 2017.5117 |
| 3.8094 | 1993.2920 | 2012.1827 | 2007.8519 |
| 3.8204 | 1953.5118 | 2002.5535 | 1998.1922 |
| 3.8314 | 2105.8476 | 1992.9247 | 1988.5325 |
| 3.8424 | 2005.4744 | 1983.2962 | 1978.8727 |
| 3.8534 | 1981.3098 | 1973.6682 | 1969.2130 |
| 3.8644 | 2020.0462 | 1964.0405 | 1959.5533 |
| 3.8754 | 1915.1475 | 1955.4240 | 1949.8935 |
| 3.8864 | 1933.6416 | 1946.9413 | 1942.3889 |
| 3.8974 | 1914.2655 | 1939.4698 | 1934.8842 |
| 3.9084 | 1988.3141 | 1931.9987 | 1927.3795 |
| 3.9194 | 1954.4071 | 1924.5281 | 1919.8748 |
| 3.9304 | 1981.2080 | 1917.0578 | 1912.3701 |
| 3.9414 | 1949.2026 | 1909.5880 | 1904.8654 |
| 3.9524 | 1969.5914 | 1902.1187 | 1897.3607 |
| 3.9634 | 1905.2950 | 1894.6498 | 1889.8560 |
| 3.9744 | 1878.0094 | 1887.1813 | 1882.3513 |
| 3.9854 | 1957.3982 | 1879.7133 | 1874.8466 |
| 3.9964 | 1934.7251 | 1872.2458 | 1867.3419 |
| 4.0074 | 1839.0669 | 1864.7788 | 1859.8372 |
| 4.0184 | 1927.4867 | 1857.3123 | 1852.3326 |
| 4.0294 | 1904.9056 | 1849.8463 | 1844.8279 |
| 4.0404 | 1817.2399 | 1842.3808 | 1837.3232 |
| 4.0514 | 1847.2743 | 1834.9159 | 1829.8185 |
| 4.0624 | 1830.3874 | 1827.4515 | 1822.3138 |
| 4.0734 | 1833.8250 | 1819.9876 | 1814.8091 |
| 4.0844 | 1818.0177 | 1812.5243 | 1807.3044 |
| 4.0954 | 1814.4474 | 1805.0616 | 1799.7997 |
| 4.1064 | 1806.4228 | 1797.5995 | 1792.2950 |
| 4.1174 | 1755.3481 | 1790.1381 | 1784.7903 |
| 4.1284 | 1776.8279 | 1782.6772 | 1777.2856 |
| 4.1394 | 1730.1436 | 1775.2170 | 1769.7809 |
| 4.1504 | 1767.2389 | 1767.7574 | 1762.2762 |
| 4.1614 | 1755.5005 | 1760.2985 | 1754.7716 |
| 4.1724 | 1783.5497 | 1752.8403 | 1747.2669 |
| 4.1834 | 1785.4690 | 1745.3828 | 1739.7622 |
| 4.1944 | 1776.3889 | 1737.9260 | 1732.2575 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 9 Etosha22 Sub 0.1-4cm S1 heat 400C | 2.0054 | 29.9894 | 0.0110 | 12/4/2023 12:12:24 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 5.3009 | 117.28 | 0.2165 | 16.65786 | 9.42 |
| 7.2452 | 1244.79 | 0.5196 | 12.19138 | 100.00 |
| 8.7363 | 496.80 | 0.1082 | 10.11363 | 39.91 |
| 13.1294 | 15.27 | 0.5196 | 6.73781 | 1.23 |
| 15.7841 | 438.00 | 0.0974 | 5.61003 | 35.19 |
| 17.6637 | 37.71 | 0.2598 | 5.01709 | 3.03 |
| 18.2396 | 50.52 | 0.1732 | 4.85995 | 4.06 |
| 19.5771 | 38.28 | 0.6061 | 4.53083 | 3.08 |
| 25.9683 | 265.87 | 0.1948 | 3.42840 | 21.36 |
| 26.7214 | 107.23 | 0.2165 | 3.33347 | 8.61 |
| 27.5209 | 39.85 | 0.2165 | 3.23841 | 3.20 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 01-071-0811 | 55 | Sodium Aluminum Silicate Hydrate | Na Al ( Si2 O6 ) ( H2 O ) | Analcime | 23 |
| * | 00-042-1339 | 26 | Potassium Magnesium Aluminum Silicate Hydroxide | K Mg3 ( Si3 Al ) O10 ( O H )2 | Phlogopite-2M1 | 22 |
| * | 01-080-5019 | 28 | Magnesium Silicate Hydroxide Hydrate | Mg7.68 ( Si12 O30 ) ( O H )4 ( H2 O )4 ( H2 O )6 | Sepiolite | 21 |
| * | 04-025-4215 | 6 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 34 |

Anchor Scan Parameters

Dataset Name	9 Etosha22 Sub 0.1-4cm S1 heat 400C

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 9\9 Etosha22 Sub 0.1-4cm S1 heat 400C.xrdml

Sample Identification	9 Etosha22 Sub 0.1-4cm S1 heat 400C

Measurement Start Date/Time	12/4/2023 12:12:24 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes