9 Etosha 22 Sub 0.1-4 cm S1 550 C

Graphics

Graphics

Graphics

Quantitative Results

Phase Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide

Weight fraction/ %	70.0

Phase Sodium Aluminum Silicate

Weight fraction/ %	7.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	22.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide | Sodium Aluminum Silicate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide |
| --- | --- | --- | --- |
| 9 Etosha22 Sub 0.1-4cm S1 heat 550C | 70.0 | 7.0 | 22.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 5288.0000 | 5288.0000 | 5288.0000 |
| 2.0164 | 5224.3328 | 5251.2478 | 5251.2478 |
| 2.0274 | 5012.3353 | 5214.4956 | 5214.4956 |
| 2.0384 | 5101.2021 | 5177.7434 | 5177.7434 |
| 2.0494 | 4998.3127 | 5140.9912 | 5140.9912 |
| 2.0604 | 4932.4695 | 5104.2390 | 5104.2390 |
| 2.0714 | 5008.8466 | 5067.4868 | 5067.4868 |
| 2.0824 | 4917.0211 | 5030.7346 | 5030.7346 |
| 2.0934 | 4897.8682 | 4993.9824 | 4993.9824 |
| 2.1044 | 4893.5398 | 4957.2302 | 4957.2302 |
| 2.1154 | 4727.8830 | 4920.4780 | 4920.4780 |
| 2.1264 | 4770.5103 | 4883.7258 | 4883.7258 |
| 2.1374 | 4755.8437 | 4846.9736 | 4846.9736 |
| 2.1484 | 4883.6770 | 4810.2214 | 4810.2214 |
| 2.1594 | 4735.8702 | 4773.4692 | 4773.4692 |
| 2.1704 | 4709.3628 | 4736.7170 | 4736.7170 |
| 2.1814 | 4662.1042 | 4699.9648 | 4699.9648 |
| 2.1924 | 4609.6858 | 4663.2126 | 4663.2126 |
| 2.2034 | 4686.6726 | 4633.2169 | 4633.2169 |
| 2.2144 | 4667.9882 | 4603.2213 | 4603.2213 |
| 2.2254 | 4577.9980 | 4573.2256 | 4573.2256 |
| 2.2364 | 4431.1268 | 4543.2300 | 4543.2300 |
| 2.2474 | 4426.2035 | 4513.2343 | 4513.2343 |
| 2.2584 | 4483.7979 | 4483.2387 | 4483.2387 |
| 2.2694 | 4420.8555 | 4453.2430 | 4453.2430 |
| 2.2804 | 4396.2345 | 4423.2474 | 4423.2474 |
| 2.2914 | 4331.5192 | 4393.2517 | 4393.2517 |
| 2.3024 | 4257.7743 | 4363.2561 | 4363.2561 |
| 2.3134 | 4311.4749 | 4333.2604 | 4333.2604 |
| 2.3244 | 4277.0998 | 4303.2648 | 4303.2648 |
| 2.3354 | 4314.5221 | 4273.2691 | 4273.2691 |
| 2.3464 | 4241.2935 | 4243.2735 | 4243.2735 |
| 2.3574 | 4262.4090 | 4213.2778 | 4213.2778 |
| 2.3684 | 4190.6224 | 4183.2822 | 4183.2822 |
| 2.3794 | 4161.6578 | 4153.2865 | 4153.2865 |
| 2.3904 | 4090.4680 | 4128.7722 | 4128.7722 |
| 2.4014 | 4089.3982 | 4104.2579 | 4104.2579 |
| 2.4124 | 4088.9779 | 4079.7436 | 4079.7436 |
| 2.4234 | 4068.1613 | 4055.2293 | 4055.2293 |
| 2.4344 | 4069.0900 | 4030.7150 | 4030.7150 |
| 2.4454 | 3990.6519 | 4006.2006 | 4006.2006 |
| 2.4564 | 3968.6377 | 3981.6863 | 3981.6863 |
| 2.4674 | 3951.9292 | 3957.1720 | 3957.1720 |
| 2.4784 | 3880.3614 | 3932.6577 | 3932.6577 |
| 2.4894 | 3855.2753 | 3908.1434 | 3908.1434 |
| 2.5004 | 3864.5531 | 3883.6291 | 3883.6291 |
| 2.5114 | 3890.4425 | 3859.1148 | 3859.1148 |
| 2.5224 | 3828.5472 | 3834.6005 | 3834.6005 |
| 2.5334 | 3843.3363 | 3810.0862 | 3810.0862 |
| 2.5444 | 3779.3658 | 3785.5718 | 3785.5718 |
| 2.5554 | 3742.3314 | 3761.0575 | 3761.0575 |
| 2.5664 | 3701.1814 | 3736.5432 | 3736.5432 |
| 2.5774 | 3755.3137 | 3716.3282 | 3716.3282 |
| 2.5884 | 3728.5260 | 3696.1132 | 3696.1132 |
| 2.5994 | 3731.1328 | 3675.8982 | 3675.8982 |
| 2.6104 | 3623.5305 | 3655.6831 | 3655.6831 |
| 2.6214 | 3699.3481 | 3635.4681 | 3635.4681 |
| 2.6324 | 3656.2109 | 3615.2531 | 3615.2531 |
| 2.6434 | 3596.0295 | 3595.0381 | 3595.0381 |
| 2.6544 | 3598.7021 | 3574.8231 | 3574.8231 |
| 2.6654 | 3586.5133 | 3554.6081 | 3554.6081 |
| 2.6764 | 3489.5300 | 3534.3930 | 3534.3930 |
| 2.6874 | 3449.8555 | 3514.1780 | 3514.1780 |
| 2.6984 | 3431.5133 | 3493.9630 | 3493.9630 |
| 2.7094 | 3438.0128 | 3473.7480 | 3473.7480 |
| 2.7204 | 3436.2065 | 3453.5330 | 3453.5330 |
| 2.7314 | 3411.4749 | 3433.3179 | 3433.3179 |
| 2.7424 | 3404.3530 | 3413.1029 | 3413.1029 |
| 2.7534 | 3415.7011 | 3393.6041 | 3392.8879 |
| 2.7644 | 3367.9631 | 3376.2622 | 3376.2622 |
| 2.7754 | 3327.1662 | 3359.6364 | 3359.6364 |
| 2.7864 | 3360.3973 | 3343.0107 | 3343.0107 |
| 2.7974 | 3312.9026 | 3326.3849 | 3326.3849 |
| 2.8084 | 3289.8496 | 3309.7591 | 3309.7591 |
| 2.8194 | 3265.2616 | 3293.1334 | 3293.1334 |
| 2.8304 | 3282.3584 | 3276.5076 | 3276.5076 |
| 2.8414 | 3220.4798 | 3259.8819 | 3259.8819 |
| 2.8524 | 3417.5856 | 3243.2561 | 3243.2561 |
| 2.8634 | 3245.8879 | 3226.6304 | 3226.6304 |
| 2.8744 | 3212.7542 | 3210.0046 | 3210.0046 |
| 2.8854 | 3203.1504 | 3193.3789 | 3193.3789 |
| 2.8964 | 3177.1150 | 3176.7531 | 3176.7531 |
| 2.9074 | 3182.1337 | 3160.1274 | 3160.1274 |
| 2.9184 | 3197.9115 | 3143.5016 | 3143.5016 |
| 2.9294 | 3144.3186 | 3126.8759 | 3126.8759 |
| 2.9404 | 3122.7473 | 3110.2501 | 3110.2501 |
| 2.9514 | 3090.9813 | 3093.6243 | 3093.6243 |
| 2.9624 | 3012.1593 | 3076.9986 | 3076.9986 |
| 2.9734 | 3069.4690 | 3060.3728 | 3060.3728 |
| 2.9844 | 3084.2158 | 3043.7471 | 3043.7471 |
| 2.9954 | 3070.6106 | 3027.1213 | 3027.1213 |
| 3.0064 | 3077.0658 | 3010.4956 | 3010.4956 |
| 3.0174 | 2902.1386 | 2993.8698 | 2993.8698 |
| 3.0284 | 2931.4410 | 2977.2441 | 2977.2441 |
| 3.0394 | 2976.5624 | 2960.6183 | 2960.6183 |
| 3.0504 | 2937.6116 | 2943.9926 | 2943.9926 |
| 3.0614 | 2894.2389 | 2927.3668 | 2927.3668 |
| 3.0724 | 2910.5379 | 2910.7411 | 2910.7411 |
| 3.0834 | 2916.5910 | 2894.1153 | 2894.1153 |
| 3.0944 | 2900.0398 | 2877.4895 | 2877.4895 |
| 3.1054 | 2840.5015 | 2860.8638 | 2860.8638 |
| 3.1164 | 2820.3102 | 2844.2380 | 2844.2380 |
| 3.1274 | 2822.8643 | 2828.5901 | 2827.6123 |
| 3.1384 | 2849.1917 | 2815.8867 | 2815.8867 |
| 3.1494 | 2808.7463 | 2804.1611 | 2804.1611 |
| 3.1604 | 2692.0413 | 2792.4355 | 2792.4355 |
| 3.1714 | 2740.8053 | 2780.7099 | 2780.7099 |
| 3.1824 | 2762.6372 | 2768.9843 | 2768.9843 |
| 3.1934 | 2702.3097 | 2757.2587 | 2757.2587 |
| 3.2044 | 2715.1917 | 2745.5331 | 2745.5331 |
| 3.2154 | 2729.7198 | 2733.8075 | 2733.8075 |
| 3.2264 | 2758.9808 | 2722.0820 | 2722.0820 |
| 3.2374 | 2803.2743 | 2710.3564 | 2710.3564 |
| 3.2484 | 2746.8889 | 2698.6308 | 2698.6308 |
| 3.2594 | 2711.1740 | 2686.9052 | 2686.9052 |
| 3.2704 | 2706.2694 | 2675.1796 | 2675.1796 |
| 3.2814 | 2686.0678 | 2663.4540 | 2663.4540 |
| 3.2924 | 2663.5885 | 2651.7284 | 2651.7284 |
| 3.3034 | 2705.3117 | 2640.0028 | 2640.0028 |
| 3.3144 | 2631.0103 | 2628.2772 | 2628.2772 |
| 3.3254 | 2581.8909 | 2616.5516 | 2616.5516 |
| 3.3364 | 2616.3053 | 2604.8260 | 2604.8260 |
| 3.3474 | 2586.9971 | 2593.1004 | 2593.1004 |
| 3.3584 | 2596.1416 | 2581.3749 | 2581.3749 |
| 3.3694 | 2610.9095 | 2569.6493 | 2569.6493 |
| 3.3804 | 2605.0541 | 2557.9237 | 2557.9237 |
| 3.3914 | 2516.1858 | 2546.1981 | 2546.1981 |
| 3.4024 | 2495.6333 | 2534.4725 | 2534.4725 |
| 3.4134 | 2568.5546 | 2522.7469 | 2522.7469 |
| 3.4244 | 2576.9203 | 2511.0213 | 2511.0213 |
| 3.4354 | 2487.2704 | 2499.2957 | 2499.2957 |
| 3.4464 | 2504.7242 | 2487.5701 | 2487.5701 |
| 3.4574 | 2485.1357 | 2475.8445 | 2475.8445 |
| 3.4684 | 2514.9140 | 2464.1189 | 2464.1189 |
| 3.4794 | 2519.7089 | 2452.3933 | 2452.3933 |
| 3.4904 | 2499.6814 | 2440.6677 | 2440.6677 |
| 3.5014 | 2433.8564 | 2429.4603 | 2428.9422 |
| 3.5124 | 2368.4902 | 2419.8131 | 2419.8131 |
| 3.5234 | 2316.1032 | 2410.6841 | 2410.6841 |
| 3.5344 | 2391.3909 | 2401.5551 | 2401.5551 |
| 3.5454 | 2423.2340 | 2392.4261 | 2392.4261 |
| 3.5564 | 2403.4071 | 2383.2971 | 2383.2971 |
| 3.5674 | 2434.2665 | 2374.1681 | 2374.1681 |
| 3.5784 | 2367.4498 | 2365.0391 | 2365.0391 |
| 3.5894 | 2319.6726 | 2355.9100 | 2355.9100 |
| 3.6004 | 2386.5271 | 2346.7810 | 2346.7810 |
| 3.6114 | 2351.3854 | 2337.6520 | 2337.6520 |
| 3.6224 | 2328.1254 | 2328.5230 | 2328.5230 |
| 3.6334 | 2330.9145 | 2319.3940 | 2319.3940 |
| 3.6444 | 2315.3727 | 2310.2650 | 2310.2650 |
| 3.6554 | 2348.2773 | 2301.1359 | 2301.1359 |
| 3.6664 | 2322.4739 | 2292.0069 | 2292.0069 |
| 3.6774 | 2272.7197 | 2282.8779 | 2282.8779 |
| 3.6884 | 2345.2478 | 2273.7358 | 2273.7489 |
| 3.6994 | 2236.3618 | 2264.5541 | 2264.5541 |
| 3.7104 | 2214.7591 | 2255.3592 | 2255.3592 |
| 3.7214 | 2146.1121 | 2246.1644 | 2246.1644 |
| 3.7324 | 2193.9223 | 2236.9696 | 2236.9696 |
| 3.7434 | 2165.0305 | 2227.7747 | 2227.7747 |
| 3.7544 | 2268.9248 | 2218.5799 | 2218.5799 |
| 3.7654 | 2205.3736 | 2209.3851 | 2209.3851 |
| 3.7764 | 2192.2325 | 2200.1902 | 2200.1902 |
| 3.7874 | 2221.7345 | 2190.9954 | 2190.9954 |
| 3.7984 | 2198.0620 | 2181.8006 | 2181.8006 |
| 3.8094 | 2216.5978 | 2172.6057 | 2172.6057 |
| 3.8204 | 2253.4675 | 2163.4109 | 2163.4109 |
| 3.8314 | 2230.5654 | 2154.2160 | 2154.2160 |
| 3.8424 | 2128.1038 | 2145.0212 | 2145.0212 |
| 3.8534 | 2183.8053 | 2135.8264 | 2135.8264 |
| 3.8644 | 2179.3790 | 2126.6315 | 2126.6315 |
| 3.8754 | 2156.3314 | 2117.4367 | 2117.4367 |
| 3.8864 | 2117.8805 | 2108.2419 | 2108.2419 |
| 3.8974 | 2110.2812 | 2099.0470 | 2099.0470 |
| 3.9084 | 2121.0506 | 2089.8522 | 2089.8522 |
| 3.9194 | 2078.8230 | 2080.6574 | 2080.6574 |
| 3.9304 | 2109.2645 | 2071.4625 | 2071.4625 |
| 3.9414 | 2085.4877 | 2062.2677 | 2062.2677 |
| 3.9524 | 2124.4366 | 2053.0729 | 2053.0729 |
| 3.9634 | 2098.8682 | 2043.8780 | 2043.8780 |
| 3.9744 | 2069.3943 | 2034.6832 | 2034.6832 |
| 3.9854 | 2031.9204 | 2025.4883 | 2025.4883 |
| 3.9964 | 2065.2247 | 2016.3356 | 2016.2935 |
| 4.0074 | 2032.3500 | 2007.2732 | 2007.0987 |
| 4.0184 | 1939.4543 | 1998.1365 | 1997.9038 |
| 4.0294 | 1970.3068 | 1988.9457 | 1988.7090 |
| 4.0404 | 1940.5138 | 1979.7550 | 1979.5142 |
| 4.0514 | 1976.1386 | 1970.5645 | 1970.3193 |
| 4.0624 | 1953.1834 | 1961.9156 | 1961.1245 |
| 4.0734 | 1950.1790 | 1953.7792 | 1953.5253 |
| 4.0844 | 2006.2964 | 1946.1846 | 1945.9260 |
| 4.0954 | 1984.4474 | 1938.5901 | 1938.3268 |
| 4.1064 | 2019.1765 | 1930.9957 | 1930.7275 |
| 4.1174 | 1968.0944 | 1923.4015 | 1923.1283 |
| 4.1284 | 1900.4209 | 1915.8074 | 1915.5291 |
| 4.1394 | 1906.0816 | 1908.2134 | 1907.9298 |
| 4.1504 | 1917.5502 | 1900.6196 | 1900.3306 |
| 4.1614 | 1904.6882 | 1893.0260 | 1892.7314 |
| 4.1724 | 1835.8535 | 1885.4325 | 1885.1321 |
| 4.1834 | 1836.0177 | 1877.8392 | 1877.5329 |
| 4.1944 | 1834.0929 | 1870.2461 | 1869.9336 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 9 Etosha22 Sub 0.1-4cm S1 heat 550C | 2.0054 | 29.9894 | 0.0110 | 12/4/2023 3:23:03 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 5.2958 | 160.77 | 0.1299 | 16.67375 | 27.89 |
| 8.7692 | 576.36 | 0.0866 | 10.07576 | 100.00 |
| 10.5757 | 40.58 | 0.2598 | 8.35836 | 7.04 |
| 15.9100 | 215.62 | 0.1299 | 5.56593 | 37.41 |
| 17.7590 | 17.71 | 0.6927 | 4.99037 | 3.07 |
| 19.8437 | 22.97 | 0.6061 | 4.47055 | 3.98 |
| 26.2553 | 145.68 | 0.3464 | 3.39157 | 25.28 |
| 27.5196 | 77.56 | 0.3464 | 3.23856 | 13.46 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-023-1515 | 37 | Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide | K0.93 Na0.05 Mg1.71 Ti0.13 Fe0.97 Al1.44 Si2.75 O10.47 ( O H )1.33 F0.2 | Phlogopite-1M | 70 |
| * | 01-073-6448 | 38 | Sodium Aluminum Silicate | Na Al ( Si2 O6 ) | Analcime | 7 |
| * | 04-025-4215 | 2 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 22 |

Anchor Scan Parameters

Dataset Name	9 Etosha22 Sub 0.1-4cm S1 heat 550C

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 9\9 Etosha22 Sub 0.1-4cm S1 heat 550C.xrdml

Sample Identification	9 Etosha22 Sub 0.1-4cm S1 heat 550C

Measurement Start Date/Time	12/4/2023 3:23:03 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes